# Q21 IN SITU CONCRETE ROADS/ PAVINGS/ BASES

To be read with Preliminaries/ General conditions.

TYPES OF PAVING

130	CONCRETE BASE FOR PAVING SLABS, BRICK MARGINS AND COBBLES

•	 Concrete: To BS 8500-2.

-	Designation: PAV2.

-	Fibres: Not required.

-	Aggregate:

Size (maximum): 20 mm.

Coarse recycled concrete aggregate: Not permitted.

Additional aggregate requirements: None.

-	Consistence class: S2.

-	Additional mix requirements: None.

GENERAL/ PREPARATION

140	READY-MIXED CONCRETE

•	 Production plant: Currently certified by a body accredited by UKAS to BS EN 45011 for

product conformity certification of ready-mixed concrete.

•	 Source of ready-mixed concrete: Obtain from one source if possible. Otherwise, submit

proposals.

-	Name and address of depot: Submit before any concrete is delivered.

-	Delivery notes: Retain for inspection.

•	 Declarations of nonconformity from concrete producer: Notify immediately.

LAYING CONCRETE

310	TRANSPORTING CONCRETE

•	 General: Avoid contamination, segregation, loss of ingredients, excessive evaporation

and loss of workability. Protect from heavy rain.

•	 Entrained air: Anticipate effects of transport and placing methods in order to achieve

specified air content.

•	 Placing: Use suitable walkways and barrow runs for traffic over reinforcement and

freshly placed concrete.

320	LAYING CONCRETE GENERALLY

•	 Timing: Place as soon as practicable after mixing and while sufficiently plastic for full

compaction. After discharge from the mixer do not add water or retemper.

•	 Temperature of concrete at point of delivery:

-	In hot weather (maximum): 30°C.

-	In cold weather (minimum): 5°C.

•	 Cold weather:

-	Do not use frozen materials.

-	Do not place concrete against frozen or frost covered surfaces.

-	Do not place concrete when air temperature is below 3°C on a falling

thermometer. Do not resume placing until rising air temperature has reached

3°C.

•	 Surfaces on which concrete is to be placed: Free from debris and standing water.

•	 Placing in final position: Place in one continuous operation up to construction joints.

-	Do not place concrete simultaneously on both sides of movement joints.

•	 Spreading: Spread and strike off with surcharge sufficient to obtain required compacted

thickness.

•	 Adjacent work: Form neat junctions and prevent damage. Keep clean all channels,

kerbs, inspection covers, etc.

330	COMPACTING

•	 General: Fully compact concrete to full depth (until air bubbles cease to appear on the

surface) especially around reinforcement, cast-in accessories, into corners and at

joints.

•	 Poker vibrators: Do not use to make concrete flow into position. Do not allow to come

into contact with fabric reinforcement.

•	 Wet formed joint grooves: Rectify any irregularities by means of a vibrating float.

•	 Finish: A dense, even textured surface free from laitance or excessive water.

-	Excess concrete: Remove from top of groove formers.

340	MANHOLE COVER AND GULLY GRATING FRAMES

•	 General: Set frames in independent concrete slabs placed over, but slightly larger than,

exterior of manhole shaft or gully pot and any concrete surround.

•	 Positioning of joints in main slab:  Set out so that manhole/ gully slabs are adjacent to a

main transverse joint, wherever possible.

•	 Joints: Separate the independent slabs from main slabs with 25 mm thick joint filler

board. Set board 20 mm below top of slab to form a sealing groove.

350	LEVELS

•	 Lines and levels of finished surface: Smooth and even, with regular falls to prevent

ponding.

•	 Finished surfaces: Within ±6 mm of required levels (+6 or -0 mm adjacent to gullies and

manholes).

JOINTS

410	JOINTS GENERALLY

•	 Layout: All joints to be accurately located, straight and well aligned.

•	 Construction joints made at end of working day: Form as contraction joints.

•	 Modifications to joint design or location: Submit proposals.

•	 Temporary support: Prior to concreting, set formwork, dowel bars, tie bars, joint filler

boards, sealing groove fillets and the like rigidly in position and support to prevent

displacement. Maintain support until concrete has set.

•	 Keep clean:

-	Do not allow concrete to enter any gaps or voids in formwork or to render

movement joints ineffective.

- Do not allow concrete to impregnate or penetrate materials used as compressible

- joint fillers.

CURING/ PROTECTION/ FINISHING

610	CURING

•	 General: Immediately after completion of surface treatment prevent evaporation from

surface and exposed edges of slabs for a minimum period of seven days.

•	 Early curing:

- Cover with waterproof sheeting held clear of surface. Seal against draughts at

- edges and junctions.

- Do not apply sprayed compounds or sheets in direct contact until surface is in a

- suitable state and will not be marked.

•	 Coverings for curing: Contractor's choice of:

-	Impervious sheet material.

-	Resin based aluminized curing compound containing a fugitive dye and with an

efficiency index of 90% when tested to BS 7542.

-	Sprayed plastics film.

660	PROTECTION

•	 Prevent damage to concrete:

-	From rain, indentation, physical damage, dirt, staining, rust marks and other

disfiguration.

-	From thermal shock.

-	In cold weather, from freezing expansion of water trapped in pockets, etc.

-	By use as a building platform or for storing, mixing or preparing materials.

670	OPENING TO TRAFFIC

•	 Light vehicles: 7 days after placing concrete.

•	 Heavy vehicles: not suitable for heavy vehicles.