# Q20 Granular sub-bases to roads/ pavings

To be read with Preliminaries/ General conditions.

110	THICKNESSES OF SUB-BASE/ SUBGRADE IMPROVEMENT LAYERS

•	 Thicknesses: See sections:

-

-  Q22 Coated macadam/ asphalt roads/ pavings;

-  Q23 Gragel/ hoggin/ woodchip roads/ pavings and

-  Q25 Slab/ brick/ sett/ cobble pavings.

140	EXCAVATION OF SUBGRADES

•	 Final excavation to formation/ subformation level: Carry out immediately before compaction

of subgrade.

•	 Soft spots and voids: Give notice.

•	 Old drainage and service trenches: Excavate to remove soft or degraded material, then

backfill with specified granular sub-base material and compact.

•	 Wet conditions: Do not excavate or compact when the subgrade may be damaged or

destabilized.

145	PREPARATION AND COMPACTION OF SUBGRADES

•	 Timing: Immediately before placing sub-base.

•	 Soft or damamged areas: Excavate and replace with sub-base material, compacted in

layers 300 mm (maximum) thick.

•	 Compaction: Thoroughly, by roller or other suitable means, adequate to resist subsidence

or deformation of the subgrade during construction and of the completed roads/ pavings

when in use. Take particular care to compact fully at intrusions, perimeters and where local

excavation and backfilling has taken place.

150	SUBGRADES FOR VEHICULAR AREAS

•	 Preparation and treatment: To Highways Agency 'Specification for highway works', clauses

616 and 617.

170	GEOTEXTILE FILTER/ SEPARATOR MEMBRANES

•	 Manufacturer: Contractor's choice.

-	Product reference: TBA.

•	 Jointing: 300 mm overlap.

•	 Protect from: -.

-	Exposure to light, except during laying (maximum five hours).

-	Contaminants.

-	Materials listed as potentially deleterious by geotextile manufacturer.

-	Damage, until fully covered by fill.

-	Wind uplift, by laying not more than 15 m before covering with fill.

•	 Preparation: Remove humps and sharp projections and fill hollows before laying.

180	NOTICE

•	 Give notice: On completion of compaction .

-	Period of notice: 5 working days.

210	HIGHWAYS AGENCY TYPE 1 GRANULAR MATERIAL

•	 Material: Type 1 unbound mixture to Highways Agency SHW clause 801.

-	Recycled aggregate: Permitted.

215A	GRANULAR MATERIAL FOR PERMEABLE PAVING

•	 Material: non-frost susceptible Type 1 granular sub-base to SHW clause 803.

225	PLACING OF MATERIAL WITH HIGH SULFATE CONTENT

•	 Standard: To Highways Agency SHW clauses 801.2 and 801.3.

-	Separation distance (minimum): 500 mm.

230	PLACING GRANULAR MATERIAL GENERALLY

•	 Preparation: Loose soil, rubbish and standing water removed.

•	 Structures, membranes and buried services: Ensure stability and avoid damage.

240	LAYING GRANULAR SUB-BASES FOR VEHICULAR AREAS

•	 General: Spread and levelled in layers. As soon as possible thereafter compact each layer.

•	 Standard: To Highways Agency 'Specification for highway works' clause 802.

•	 At drainage fittings, inspection covers, perimeters and where local excavation and

backfilling has taken place: Take particular care to compact fully.

250	LAYING GRANULAR SUB-BASESFOR PEDESTRIAN AREAS

•	 General: Spread and levelled.

•	 Compaction:

-	Timing: As soon as possible after laying.

-	Method: By roller or other suitable means, adequate to resist subsidence or deformation

of the sub-base during construction and of the completed paving when in use. Take

particular care to compact fully at intrusions, perimeters and where local excavation and

backfilling has taken place.

310	ACCURACY

•	 Permissible deviation from required levels, falls and cambers (maximum):

-	Subgrades:

Roads and parking areas: +20 -30 mm.

Footways and recreation areas: ±0 mm.

-	Sub-bases:

Roads and parking areas: ±0 mm.

-	Footways and recreation areas: ±2 mm .

330	COLD WEATHER WORKING

•	 Frozen materials: Do not use.

•	 Freezing conditions: Do not place fill on frozen surfaces. Remove material affected by

frost. Replace and recompact if not damaged after thawing.

340	PROTECTION

•	 Sub-bases: As soon as practicable, cover with subsequent layers, specified elsewhere.

•	 Subgrades and sub-bases: Prevent degradation by construction traffic, construction

operations and inclement weather.