M10	CEMENT BASED LEVELLING / WEARING SCREEDS

To be read with Preliminaries/ General conditions.

TYPES OF SCREED

M10/110	BONDED CEMENT:SAND LEVELLING SCREEDS AREAS G13 & G23, AND ELSEWHERE WHERE MAKING GOOD REQUIRED TO EXISTING FLOORS

-	Substrate: existing concrete slab.

DPM: cold bituminous liquid applied damp proofing, contractor’s choice

-	Screed construction: Fully bonded.

-	Thickness:

-	Minimum: 25 mm.

-	Maximum: 40 mm.

-	Mix:

-	Proportions (cement:sand): manufacturer’s standard.

-	In situ crushing resistance (ISCR) category: B .

-	Flatness/ Surface regularity: Maximum permissible deviation: to suit floor covering .

-	Finish: Trowelled as clause 540 .

-	To receive: carpet, sheet linoleum, quarry tiles, timber boards on battens .

M10/130	PROPRIETARY QUICK DRYING LEVELLING SCREED AREAS G01-G04, G07, G07, G09, G14, G15, G17, G20

-	Substrate: beam and block floor, see engineers specification.

-	Screed manufacturer: Contractor’s choice.

-	Product reference: To Architect’s approval.

-	Screed construction: Floating as clause 290.

-	Reinforcement for crack control: As recommended by manufacturer.

-	Thickness:

-	Nominal: 95mm.

-	Minimum: 75mm .

-	Mix:

-	Cement: Manufacturer's standard..

-	Proportions: Manufacturer's standard.

-	In situ crushing resistance (ISCR) category: A (see BS 8204-1 Annex E-floating) .

-	Mass of test weight: 4kg.

-	Flatness/ Surface regularity: Maximum permissible deviation: 3 mm under a 3 m straight edge.

-	Finish:

-	Trowelled, as clause 540.

-	To receive: finishes as shown on drawings .

-	Other requirements: Expansion joints in accordance with manufacturer’s recommendations and requirements of underfloor heating; Underfloor heating as mechanical specification.

GENERALLY/ PREPARATION

210	SUITABILITY OF BASES

-	General:

-	Suitable for specified levels and flatness/ regularity of finished surfaces. Consider permissible minimum and maximum thicknesses of screeds.

-	Sound and free from significant cracks and gaps.

-	Cleanliness: Remove plaster, debris and dirt.

-	Moisture content: To suit screed type. New concrete slabs to receive fully or partially bonded construction must be dried out by exposure to the air for minimum six weeks.

220	PROPRIETARY LEVELLING/ WEARING SCREEDS

-	General: Materials, mix proportions, mixing methods, minimum/ maximum thicknesses and workmanship must be in accordance with recommendations of screed manufacturer.

-	Standard: To BS 8204-3.

250	CONDUITS UNDER FLOATING SCREEDS

-	Haunching: Before laying insulation for floating screeds, haunch up in 1:4 cement:sand on both sides of conduits.

251	CONDUITS CAST INTO OR UNDER SCREEDS

-	Reinforcement: Overlay with reinforcement selected from:

-	500 mm wide strip of steel fabric to BS 4483, reference D49, or

-	Welded mesh manufactured in rolls from mild steel wire minimum than 1.5 mm diameter to BS 1052, mesh size 50 x 50 mm.

-	Placing reinforcement: Mid depth between top of conduit and the screed surface.

-	Screed cover over conduit (minimum): 25 mm.

290	FLOATING CONSTRUCTION

-	Location: Throughout new extension.

- Insulation: Separation layer on 60m thick Kingspan Styrozone H-500R.

- Installation: Lay with tight butt joints. Continue lesser thickness of insulation up at perimeter abutments for full depth of screed.

Separating layer:

- Type: 500 gauge polyethylene sheet

- Installation: Lay over insulation and turn up at perimeter abutments. Lap 100 mm at joints.

BATCHING/ MIXING

M10/302	CEMENTS

-	Cement types: In accordance with BS 8204-1, clause 5.1.3.

M10/305	AGGREGATES

-	Sand: To BS EN 13139.

-	Grading limits: In accordance with BS 8204-1, Table B1.

-	Coarse aggregates for fine concrete levelling screeds:

-	Standard: To BS EN 12620.

-	Designation 4/10.

-	Lightweight aggregates: To BS 8204-1, Annex A.

M10/307	ADMIXTURES

-	Standard: In accordance with BS 8204-1, Table 1.

-	Calcium chloride: Do not use in admixtures.

M10/310	BATCHING WITH DENSE AGGREGATES

-	Mix proportions: Specified by weight.

-	Batching: Select from:

-	Batch by weight.

-	Batch by volume: Permitted on the basis of previously established weight:volume relationships of the particular materials. Use accurate gauge boxes. Allow for bulking of damp sand.

M10/330	MIXING

-	Water content: Minimum necessary to achieve full compaction, low enough to prevent excessive water being brought to surface during compaction.

-	Mixing: Mix materials thoroughly to uniform consistency. Mixes other than no-fines must be mixed in a suitable forced action mechanical mixer. Do not use a free fall drum type mixer.

-	Consistency: Use while sufficiently plastic for full compaction.

-	Ready-mixed retarded screed mortar: Use within working time and site temperatures recommended by manufacturer. Do not retemper.

M10/335	IN SITU CRUSHING RESISTANCE (ISCR)

-	Standards and category: To BS 8204-1, table 4.

-	Testing of floating levelling screeds: To Annex E.

M10/340	ADVERSE WEATHER

-	Screeds surface temperature: Maintain above 5° C for a minimum of four days after laying.

-	Hot weather: Prevent premature setting or drying out.

LAYING

M10/350	SCREEDING TO FALLS

-	Minimum screed cover: Maintain at the lowest point.

-	Falls: Gradual and consistent.

-	Gradient (minimum): 1 in 80 .

M10/355	FLATNESS/ SURFACE REGULARITY OF FLOOR SCREEDS

-	Standard: To BS 8204-1, Table 5.

-	Test: To BS 8204-1, Annex C.

-	Sudden irregularities: Not permitted.

M10/375	COMPACTION OF SCREEDS

-	General: Compact thoroughly over entire area.

-	Screeds over 50 mm thick: Lay in two layers of approximately equal Thickness:. Roughen surface of compacted lower layer then immediately lay upper layer.

M10/392	GENERAL REINFORCEMENT

-	Steel fabric: To manufacturer’s recommendations.

-	Installation: In accordance with BS 8204-1.

M10/405	JOINTS IN LEVELLING SCREEDS GENERALLY

-	Laying screeds: Lay continuously using 'wet screeds' between strips or bays. Minimize defined joints.

-	Daywork joints: Form with vertical edge.

FINISHING/ CURING

M10/510	FINISHING GENERALLY

-	Timing: Carry out all finishing operations at optimum times in relation to setting and hardening of screed material.

-	Prohibited treatments to screed surfaces:

-	Wetting to assist surface working.

-	Sprinkling cement.

M10/540	TROWELLED FINISH TO LEVELLING SCREEDS

-	Floating: To an even texture with no ridges or steps.

-	Trowelling: To a uniform, smooth but not polished surface, free from trowel marks and other blemishes, and suitable to receive specified flooring material.

M10/650	CURING

-	General: Prevent premature drying. Immediately after laying, protect surface from wind, draughts and strong sunlight. As soon as screed has set sufficiently, closely cover with polyethylene sheeting.

-	Curing period (minimum): Keep polyethylene sheeting in position for period recommended by screed manufacturer.

-	Drying after curing: Allow screeds to dry gradually. Do not subject screeds to artificial drying conditions that will cause cracking or other shrinkage related problems.