Z10	PURPOSE MADE JOINERY

To be read with Preliminaries/ General conditions.

Z10/110	FABRICATION

-	Standard: To BS 1186-2.

-	Sections: Accurate in profile and length, and free from twist and bowing. Formed out of solid unless shown otherwise.

-	Machined surfaces: Smooth and free from tearing, wooliness, chip bruising and other machining defects.

-	Joints: Tight and close fitting.

-	Assembled components: Rigid. Free from distortion.

-	Screws: Provide pilot holes.

-	Screws of 8 gauge or more and screws into hardwood: Provide clearance holes.

-	Countersink screws: Heads sunk at least 2 mm below surfaces visible in completed work.

Z10/120	CROSS SECTION DIMENSIONS OF TIMBER

-	General: Dimensions on drawings are finished sizes.

-	Maximum permitted deviations from finished sizes:

-	Softwood sections: To BS EN 1313-1:-

Clause 6 for sawn sections.

Clause NA.2 for further processed sections.

-	Hardwood sections: To BS EN 1313-2:-

Clause 6 for sawn sections.

Clause NA.3 for further processed sections.

Z10/130	PRESERVATIVE TREATED WOOD

-	Cutting and machining: Completed as far as possible before treatment.

-	Extensively processed timber: Retreat timber sawn lengthways, thicknessed, planed, ploughed, etc.

-	Surfaces exposed by minor cutting and/ or drilling: Treat with two flood coats of a solution recommended by main treatment solution manufacturer.

Z10/140	MOISTURE CONTENT

-	Wood and wood based products: Maintain within range specified for the component during manufacture and storage.

Z10/250	FINISHING

-	Joinery surfaces: Smooth, even and suitable to receive finishes.

-	Arrises: Eased unless shown otherwise on drawings.

-	End grain in external components: Sealed with primer or sealer as section M60 and allowed to dry before assembly.