Z12	PRESERVATIVE / FIRE RETARDANT TREATMENT

To be read with Preliminaries/ General conditions.

Z12/110	TREATMENT APPLICATION

-	Timing: After cutting and machining timber, and before assembling components.

-	Processor: Licensed by manufacturer of specified treatment solution.

-	Certification: For each batch of timber provide a certificate of assurance that treatment has been carried out as specified.

Z12/120	COMMODITY SPECIFICATIONS

-	Standard: Current edition of the British Wood Preserving and Damp-proofing Association (BWPDA) Manual.

Z12/130	PRESERVATIVE TREATMENT SOLUTION STRENGTHS/ TREATMENT CYCLES

-	General: Select to achieve specified service life and to suit treatability of specified wood species.

Z12/140	COPPER-ORGANIC PRESERVATIVE TREATMENT

-	Solution:

-	Manufacturer: Contractor’s choice .

-	Application: High pressure impregnation.

-	Moisture content of wood at time of treatment: Not more than 28%. After treatment, allow timber to dry before using.

Z12/210	FIRE RETARDANT TREATMENT

-	Solution type:.

-	Manufacturer Contractor’s choice.

-	Application: Vacuum + pressure impregnation.

-	Moisture content of wood at time of treatment: As specified for the timber/ component at time of fixing. After treatment, timber to be redried slowly at temperatures not exceeding 65°C to minimize distortion and degradation.

Z12/220	LEACH RESISTANT FIRE RETARDANT TREATMENT

-	Solution:

-	Manufacturer Contractor’s choice.

-	Application: Vacuum + pressure impregnation.

-	Moisture content of wood at time of treatment: As specified for the timber/ component at time of fixing.