Z22	SEALANTS

To be read with Preliminaries/General conditions.

Z22/120	SUITABILITY OF JOINTS

-	Presealing checks:

-	Joint dimensions: Within limits specified for the sealant.

-	Substrate quality: Surfaces regular, undamaged and stable.

-	Joints not fit to receive sealant: Submit proposals for rectification.

Z22/130	PREPARING JOINTS

-	Surfaces to which sealant must adhere:

-	Remove temporary coatings, tapes, loosely adhering material, dust, oil, grease, surface water and contaminants that may affect bond.

-	Clean using materials and methods recommended by sealant manufacturer.

-	Vulnerable surfaces adjacent to joints: Mask to prevent staining or smearing with primer or sealant.

-	Primer, backing strip, bond breaker: Types recommended by sealant manufacturer.

-	Backing strip and/or bond breaker installation: Insert into joint to correct depth, without stretching or twisting, leaving no gaps.

-	Protection: Keep joints clean and protect from damage until sealant is applied.

Z22/160	APPLYING SEALANTS

-	Substrate: Dry (unless recommended otherwise) and unaffected by frost, ice or snow.

-	Environmental conditions: Mix and apply primers and sealants within temperature and humidity ranges recommended by manufacturers. Do not dry or raise temperature of joints by heating.

-	Sealant application: Unless shown otherwise on drawings, fill joints completely and neatly, ensuring firm adhesion to substrates.

-	Sealant profiles:

-	Butt and lap joints: Slightly concave.

-	Fillet joints: Flat or slightly convex.

-	Protection: Protect finished joints from contamination or damage until sealant has cured.