# Q22 Asphalt roads/ pavings

To be read with Preliminaries/ General conditions.

TYPES OF PAVING

110	ASPHALT CONCRETE PAVING - WHERE NOTED AS BITMAC ON DRAWINGS

•	 Standard: To Highways Agency (HA) 'Specification for highway works'.

•	 Subgrade improvement layer: Not required.

-	Compacted thickness: Not applicable.

•	 Granular sub-base: As section Q20.

-	Compacted thickness: 150 mm.

•	 Base: Dense asphalt concrete to HA clause 906.

-	Paving grade: Not applicable.

-	Compacted thickness: 70-150 mm nominal, 55 mm minimum at any point.

•	 Binder course: Dense asphalt concrete to HA clause 906.

-	Paving grade: Not applicable.

-	Compacted thickness: 65 mm.

•	 Surface course: Close graded asphalt concrete to HA clause 909.

-	Paving grade: Not applicable.

-	Compacted thickness: 20-30 mm nominal, 15 mm minimum at any point.

•	 Reclaimed content:

-	Standard: To BS EN 13108-8.

-	Value (maximum): Surface course 10%, other courses 50%.

•	 Surface treatment: to match existing.

•	 Other requirements: As HA Appendix 7/1.

180	SURFACE TREATMENT TO EXISTING PAVINGADJACENT TO NEW ROADWAY

•	 Base: Existing asphalt concrete.

•	 Preparation: Cut out depressions, fill to match existing surface and compact.

•	 Surface to receive dressing: Clean and dry. All patching complete.

•	 Binder: Bitumen emulsion.

•	 Finish: to match existing.

LAYING

310	LAYING GENERALLY

•	 Preparation: Remove all loose material, rubbish and standing water.

•	 Adjacent work: Form neat junctions. Do not damage.

•	 Channels, kerbs, inspection covers etc: Keep clean.

•	 New paving:

-	Keep traffic free until it has cooled to prevailing atmospheric temperature.

-	Do not allow rollers to stand at any time.

-	Prevent damage.

-	Lines and levels: With regular falls to prevent ponding.

-	Overall texture: Smooth, even and free from dragging, tearing or segregation.

-	State on completion: Clean.

330	LEVELS

•	 Permissible deviation from the required levels, falls and cambers (maximum): In

accordance with BS 594987, Table 7.

351	CONTRACTOR'S USE OF PAVEMENTS

•	 Preparation for final surfacing:

-	Timing: Defer laying until as late as practicable.

-	Immediately before laying final surfacing: Clean and make good the base/ binder course.

Allow to dry.

-	Adhesion: Tack coat to BS 434-1 or BS EN 13808.

Application rate: As manufacturer's recommendation.

Accuracy: Uniform, without puddles.

-	Finishing: Allow emulsion to break completely before applying surface.