Z31	POWDER COATINGS

To be read with Preliminaries/ General conditions.

Z31/120	POWDER COATING MATERIALS

-	Manufacturer: Obtain from one only of the following:

Syntha Pulvin or equal approved.

-	Selected manufacturer: Submit details before commencement of powder coating.

Z31/210	WORKING PROCEDURES

-	Requirement: Comply with:

-	BS 6496 for aluminium alloy backgrounds.

-	BS 6497 for galvanized steel backgrounds.

-	British Coatings Federation: Code of safe practice - Application of thermosetting powder coatings by electrostatic spraying.

-	Powder coating manufacturer’s guarantee.

Z31/220	POWDER COATING APPLICATORS

-	Applicator requirements:

-	Approved by powder coating manufacturer.

-	Currently certified to BS EN ISO 9001.

-	Comply with quality procedures, guarantee conditions, standards and tests required by powder coating manufacturer.

-	Each applicator to use only one plant.

-	Selected applicator: Submit details before commencement of powder coating.

Z31/225	GUARANTEES

-	Powder coating manufacturer and applicator guarantees:

-	Submit sample copies before commencement of powder coating.

-	Submit signed project specific copies on completion of work.

Z31/310	PRETREATMENT

-	Condition of components to be powder coated:

-	Free from corrosion and damage.

-	Free from impurities including soil, grease, oil.

-	Suitable for and compatible with the pretreatment and powder coating process.

-	Process: Clean, conversion coat, condition, rinse in demineralised water, drain and dry components in accordance with the powder coating manufacturer’s requirements and the pretreatment supplier’s recommendations.

Z31/430	EXTENT OF POWDER COATINGS

-	Application: To visible component surfaces, and concealed surfaces requiring protection. Coated surfaces will be deemed ‘significant surfaces’ for relevant BS 6496/ BS 6497 performance requirements.

Z31/435	APPLICATION OF POWDER COATINGS

-	Surfaces to receive powder coatings: Free from dust or powder deposits.

-	Completion of powder coatings: Within 48 hours of pre-treatment of components.

-	Jig points: Not visible on coated components.

-	Curing: Controlled to attain metal temperatures and hold periods recommended by powder coating manufacturer.

-	Stripping and recoating of components: Only acceptable by prior agreement of powder coating manufacturer. Stripping, pretreatment and powder coating are to be in accordance with manufacturer’s requirements.

-	Overcoating of components: Not acceptable.

Z31/440	PERFORMANCE AND APPEARANCE OF POWDER COATINGS

-	Standard: To BS 6496/ BS 6497.

Z31/450	ALUMINIUM ALLOY FABRICATIONS

-	Units may be assembled:

-	Before powder coating.

-	From components powder coated after cutting to size.

-	Where approved, from components powder coated before cutting to size.

-	Exposure of uncoated background metal: Not acceptable.

-	Assembly sealants: Compatible with powder coatings. Obtain approval of colour if sealants are visible after fabrication.

Z31/460	STEEL FABRICATIONS

-	Unit assembly: Wherever practical, before powder coating.

-	Exposure of uncoated background metal: Not acceptable.

-	Assembly sealants: Compatible with powder coatings. Obtain approval of colour if sealants are visible after fabrication.

Z31/470	FIXINGS

-	Exposed metal fixings: Powder coat together with components, or coat with matching repair paint system applied in accordance with the powder coating manufacturer’s recommendations.

Z31/480	FABRICATION DAMAGE REPAIR/ REPLACEMENT

-	Inspection: Check all components before delivery to site for damage to powder coatings. Submit proposals for repair or replacement.

Z31/510	PROTECTION

-	Powder coated surfaces of components: Protect from damage during handling and installation, or by subsequent site operations.

-	Protective coverings: Must be:

-	Resistant to weather conditions.

-	Partially removable to suit building in and access to fixing points.

-	Protective tapes in contact with powder coatings: Must be:

-	Low tack, self adhesive and light in colour.

-	Applied and removed in accordance with tape and powder coating manufacturers’ recommendations. Do not use solvents to remove residues as these are detrimental to the coating.

-	Inspection of protection: Carry out monthly. Promptly repair any deterioration or deficiency.

Z31/530	SITE DAMAGE REPAIR/ REPLACEMENT

-	Damage to powder coatings: Rectify immediately damage caused during handling and installation, or by subsequent site operations. Submit proposals for extensive repair or replacement.

Z31/535	DOCUMENTATION

-	Submit the following information for each batch of powder coated components:

-	Supplier.

-	Trade name.

-	Colour.

-	Type of powder.

-	Method of application.

-	Batch and reference number.

-	Statutory requirements.

Z31/540	COMPLETION

-	Cleaning and maintenance of powder coatings: Carry out in accordance with procedures detailed in powder coating manufacturer and applicator guarantees.