H20	RIGID SHEET CLADDING

To be read with Preliminaries/ General conditions.

TYPE(S) OF SHEET CLADDING

H20/155	PLYWOOD UPSTANDS AT ROOF ABUTMENTS AGAINST STUDWORK & BRICKWORK.  REFER TO DRAWINGS

-	Substrate: 15mm Hunton Bitroc or brickwork

-	Support system: pre-treated timber battens, all site-cut ends to be liberally brushed with additional preservative.

-	Battens:

- Size: 25 x 50mm with chamfered top & bottom ends.

- Centres: max. 400 mm

- Fasteners: 69mm D head annular ringed shank stainless steel nails @ max. 400 mm cc.

-	Breather membrane: not required.

-	Cavity barriers: not required.

-	Thermal insulation: not required.

- 	Vapour control layer: not required.

-	Board/ Sheet:

-	Manufacturer: Contractor’s choice.

Product reference: Exterior-grade plywood to BS EN 636 Pt.3.

-	Thickness: 19mm, all site-cut ends to be liberally brushed with clear preservative.

- Moisture content at time of fixing: 13 – 19%

-	Fasteners: 44mm D head annular ringed shank stainless steel nails @ 150mm cc on edges and max. 300mm cc elsewhere, min. 9mm from edges and 15mm from corners. Nails to be driven marginally below surface.

156	HORIZONTAL PLYWOOD EAVES BOARDS ABOVE TIMBER BOARDING

-	Substrate: Vertical timber weatherboarding

- -	Support system: pre-treated timber wall plate

-	Breather membrane: not required.

-	Cavity barriers: not required.

-	Thermal insulation: not required.

- 	Vapour control layer: not required.

-	Board/ Sheet:

-	Manufacturer: Contractor’s choice.

Product reference: Exterior-grade Douglas Fir plywood to BS EN 636 Pt.3.

-	Thickness: 19mm, with chamfered bottom edge, all site-cut ends to be liberally brushed with clear preservative.

- Finish/ Colour: G1S (good one side) sanded appearance-grade panels, Canply-certified or approved equivalent.

- Moisture content at time of fixing: 13 – 19%

-	Fasteners: 50mm D head annular ringed shank stainless steel nails @ 150mm cc, min. 9mm from edges and 15mm from corners. Nails to be driven marginally below surface.

157	HORIZONTAL SW EAVES BOARDS ABOVE BRICKWORK

-	Substrate: Concrete roof deck

-	Support system: pre-treated timber battens, all site-cut ends to be liberally brushed with additional preservative.

- Size: 35 x 50mm vertical battens, with chamfered bottom ends.

- Centres: max. 400 mm

- Fasteners: 100mm D head annular ringed shank stainless steel nails @ max. 400 mm cc.

-	Breather membrane: not required.

-	Cavity barriers: not required.

-	Thermal insulation: not required.

- 	Vapour control layer: not required.

-	Board/ Sheet:

-	Manufacturer: Contractor’s choice, sw board.

-	Thickness: 19mm, with chamfered bottom edge, all site-cut ends to be liberally brushed with clear preservative.

- Moisture content at time of fixing: 13 – 19%

-	Fasteners: 50mm D head annular ringed shank stainless steel nails @ 150mm cc, min. 9mm from edges and 15mm from corners. Nails to be driven marginally below surface.

GENERAL REQUIREMENTS

H20/230	TIMBER BATTENS AND COUNTERBATTENS

-	General: Regularized softwood free from decay, insect attack (except ambrosia beetle damage) and with no knots wider than half the width of the section.

-	Preservative treatment: As section Z12 and British Wood Preserving and Damp-proofing Association Commodity Specification C8.

-	Type: Tanalith E.

- Moisture content at time of fixing (maximum): 19%.

H21/142	FIXING BATTENS TO COUNTERBATTENS

-	Setting out: In straight, horizontal lines. Align on adjacent areas.

-	Batten/ Counterbatten length (minimum): 1200 mm.

-	Joints: Square cut, butted centrally on counterbattens and not occurring more than once in any group of four battens on any one counterbatten.

-	Installation: Fix each batten to each counterbatten. Use splay fixings at joints. Fastener heads to finish flush with or slightly below batten face.

H20/240	TREATED TIMBER

-	Exposed cut and drilled surfaces: Treat with two flood coats of a solution recommended for the purpose by main treatment solution manufacturer.

H20/260	FIXING SHEETS

-	General: Secure to supports without producing distortion.

-	Fasteners: Evenly spaced in straight lines, in pairs across joints and sufficient distance from edge of sheet to prevent damage.