# Q23 Gravel/ hoggin/ woodchip roads/ pavings

To be read with Preliminaries/ General conditions.

TYPES OF SURFACING

200	RESIN BOUND PAVING FOR PEDESTRIAN AREAS - FRONT ENTRANCE AND

NURSERY PLAYGROUND

Manufacturer: Sureset or similar approved

•	 Granular sub-base: Highways Agency Type 1 granular material, as section Q20.

-	Compacted thickness: 150mm.

•	 Base course:

-	Binder: 50mm AC14 close surf asphalt concrete max 160/220 pen to BS EN 13108-1:2006

-	Application: Well compacted layers to mimimum 1.5:100 falls

•	 Surface course:

-	Aggregate: TBA

-	Thickness: As recommended by manufacturer

-	Application: Hand applied and trowelled to a smooth finish

Completion: Fine sand cast onto cured surface

Other requirements: To be installed by subcontractor approved by manufacturer

210	BONDED RUBBER CHIPPINGS FOR SOFT PLAY AREA IN NURSERY PLAYGROUND

Manufacturer: Abacus Playgrounds or similar approved

Granular sub-base: Highways Agency Type 1 granular material, as section Q20.

-	Compacted thickness: 150.

Finish: minimum 20mm base and 20mm wear coat

Colour: TBA

Other requirements: To be installed by subcontractor approved by manufacturer

LAYING

340	LAYING GENERALLY

•	 Channels, gullies, etc: Keep clear.

•	 Finished surfaces:

-	Lines and levels: To prevent ponding.

-	Overall texture: Even.

-	State at completion: Clean.

350	COLD WEATHER WORKING

•	 Frozen materials: Do not use.

•	 Freezing conditions: Do not lay pavings.

•	 Cold bituminous surface dressings: Do not apply when ambient temperature is below

10°.

360A	DRAINAGE FALLS

•	 -  Falls and cross falls (minimum): 1:60.

390	PROTECTION FROM TRAFFIC AND PLANT

•	 Paved areas: Restrict access to prevent damage.