F30	ACCESSORIES/ SUNDRY ITEMS FOR BRICK/ BLOCK/ STONE WALLING

To be read with Preliminaries/ General conditions.

CAVITIES

F30/110	CONCRETE FILL TO BASE OF CAVITY

-	Concrete generally: To BS EN 206-1 and BS 8500-2.

-	Designated concrete: see structural engineer’s specification.

Workability: High.

-	Extent: Refer to detail drawing LS/WD/200.

-	Placement: Compact to eliminate voids.

F30/120	CLEANLINESS

-	Cavity base and faces, ties, insulation and exposed dpcs: Free from mortar and debris.

F30/132	PERPEND JOINT PLASTICS WEEP HOLES

-	Manufacturer: Rytons Building Products Ltd. or similar approved.

- Product reference: Rytweep.

- Colour: Terracotta.

-	Locations: Through outer leaf immediately above base of cavity, at cavity trays, stepped dpcs and external openings. 75 mm above top of cavity fill at base of cavity.

-	Provision: At not greater than 1000 mm centres and not less than two over each opening.

F30/150	FULL FILL CAVITY INSULATION

-	Insulation: Mineral wool batts (slabs).

-	Standard: to BS EN 13162 or Agrément certified.

-	Manufacturer: Rockwool Ltd.

-	Product reference: Rockwool Cavity.

-	Face size (nominal length x width): 1200 x 455mm.

-	Thickness (nominal): 100mm.

-	Thermal conductivity: 0.037W/mK.

-	Reaction to fire class: A1.

-	Additional requirements: None.

-	Placement: Continuous and free of mortar and debris.

F30/165	GRATINGS/ VENTILATORS IN INTERNAL WALLING FOR LIFT SHAFT VENTILATION

-	Standard: To BS 493, class 2.

-	Manufacturer: Contractor’s choice .

-	Product: intumescent airbrick on inside face of shaft, schoolboard pattern CI airbrick on corridor side.

-	Apertures: 225 X 225 .

-	Placement: Built in with no gaps at joints.

F30/171	VENTILATION DUCTS IN EXTERNAL WALLING

-	Manufacturer: Rytons or similar approved.

- Product reference: Rytons periscope Underfloor ventilator.

-	Placement: Across cavity, sloping away from inner leaf. Full mortar joints to seal cavity.

- 	Accessories:

- Rytons multifix airbrick, colour blue/black

- Rytons periscope vertical extension

F30/181	CAVITY CLOSERS TO PARAPETS.

- Galvanised steel plate to Structural Engineer’s details – see drawings.

REINFORCING/ FIXING ACCESSORIES

F30/220	WALL TIES FOR MASONRY CAVITY WORK

-	To structural engineer’s spec.

F30/228	FIXING TIES IN MASONRY CAVITY WALLS WITH FULL FILL CAVITY INSULATION

-	Embedment in mortar beds (minimum): 50 mm.

-	Placement: Sloping slightly downwards towards outer leaf, without bending. Drip centred in the cavity and pointing downwards.

-	Spacing: Staggered in alternate courses.

-	Horizontal centres: 750mm.

-	Vertical centres: 450mm.

-	Provision of additional ties:

One row to support lowest row of insulation batts.

Within 225 mm of reveals of unbonded openings.

Spacing: At not more than 300mm centres vertically.

F30/241	WALL STARTERS/ CONNECTORS

-	Manufacturer: Furfix or equal approved

-	Product reference: 1FUR5100 for internal leaf and 1FUR100S for external leaf

-	Material/ finish: glavanised where internal, stainless steel where external

-	Sizes: to suit 140mm leaf thickness where internal, 103mm where external

-	Sealant to external vertical joint

-    Joint preparation and sealent application: As section Z22.

F30/270	MESHWORK JOINT REINFORCEMENT IN 215MM SOLID BRICKWORK CONSTRUCTED OF 2 STRETCHER SKINS

-	Standard: To BS EN 845-3.

-	Manufacturer: Contractor’s choice to PIFA Standard 6/83A or Agrément certified..

-	Type: welded wire.

-	Material: stainless steel.

-	Width: Approximately 40-50 mm less in width than wall or leaf.

-	Placement: Lay on an even bed of mortar in a continuous strip with full laps at angles. Keep back 20 mm from face of external work, 12 mm back from face of internal work and finish joint to normal thickness.

-	Lap length (minimum): as manufacturer’s recommendations.

FLEXIBLE DAMP PROOF COURSES/ CAVITY TRAYS

F30/310	DAMP PROOF COURSE – SAND FACED AND BITUMEN BASED BELOW BRICK ON EDGE COPINGS

-	Standard: To BS 6398.

-	Manufacturer: Contractors’ choice .

F30/330	DAMP PROOF COURSE AND SITE FORMED FLEXIBLE SHEET CAVITY TRAYS.

-	Manufacturer: Ruberoid .

-	Product reference: Hyload.

INSTALLATION OF DPCS/ CAVITY TRAYS

F30/415	HORIZONTAL DPCS

-	Placement: In continuous lengths on full even bed of fresh mortar, with 100 mm laps at joints and full laps at angles.

-	Width: At least full width of leaf unless otherwise specified. Edges of dpc not covered with mortar or projecting into cavity.

-	Overlying construction: Immediately cover with full even bed of mortar to receive next masonry course.

-	Overall finished joint thickness: As close to normal as practicable.

F30/425	GROUND LEVEL DPCS

-	Joint with damp proof membrane: Continuous and effectively sealed.

F30/455	COPING/ CAPPING DPCS

-	Placement: Bed in one operation to ensure maximum bond between masonry units, mortar and dpc.

-	Dpcs crossing cavity: Provide rigid support to prevent sagging.

F30/465	SEALING DPCS  GENERALLY

-	Overlaps and junctions: Seal with Ruberoid Hyload lap adhesive.

F30/475	SITE FORMED CAVITY TRAYS

-	Requirements to prevent downward ingress of water:

-	Profiles: To match those shown on drawings. Firmly secured.

-	Joint treatment: Use unjointed wherever possible, otherwise lap at least 100 mm and seal to produce a free draining and watertight installation.

-	Horizontal cavity trays: Support using cavity closer.

-	Sloping cavity trays: Prevent sagging.

-	Cleanliness: Free from debris and mortar droppings.

F30/485	CAVITY TRAYS OVER OPENINGS AND OTHER CAVITY BRIDGINGS

-	Length: To extend not less than 150 mm beyond ends of lintels/ bridgings.

F30/515	DPC/ CAVITY TRAY LEADING EDGE IN FACEWORK - FLUSH

-	Treatment at face of masonry: Finish flush and clear of mortar at the following locations: ground level DPC.

F30/525	DPC/ CAVITY TRAY LEADING EDGE IN FACEWORK - SET BACK

-	Treatment at face of masonry: Set back 5 mm from face of wall with recessed mortar joint to expose edge at the following locations: above windows and doors.

F30/560	VERTICAL DPCS GENERALLY

-	Form: In one piece wherever possible.

-	Joints: Upper part overlapping lower not less then 100 mm.

F30/570	JAMB DPCS AT OPENINGS

-	Joint with cavity tray/ lintel at head: Full underlap.

-	Joint with sill/ horizontal dpc at base: Full overlap.

-	Projection into cavity: Not less than 25 mm.

-	Relationship with frame: In full contact.

F30/580	JAMB DPCS TO BUILT IN TIMBER FRAMES

-	Fixing: Securely fastened to back of frame.

-	Fasteners: Galvanized clout nails or staples.

JOINTS

F30/610	EXTERNAL MOVEMENT JOINTS WITH SEALANT

-	Joint preparation and sealant application: As section Z22.

-	Filler: closed cell polyethylene.

-	Thickness: To match design width of joint.

-	Manufacturer: Grace Building Products Ltd. or similar approved.

Product reference: 10mm Aerofil.

-	Placement: Build in as work proceeds with no projections into cavities and to correct depth to receive sealant system.

-	Sealant: 20mm deep x 10mm Vertiseal polysulphide sealant

-	Colour: to match brickwork

F30/650	POINTING IN FLASHINGS

-	Joint preparation: Free of debris and lightly wetted.

-	Pointing mortar: As for adjacent walling.

-	Placement: Fill joint and finish flush.

F30/660	PINNING UP TO SOFFITS

-	Top joint of loadbearing walls: Fill and consolidate with mortar.

F30/670	TOPS OF NONLOADBEARING WALLS

-	Restraints: 50 x 50mm continuous softwood battens fixed at 600mm centres with 14 gauge screws.

-	Fixing: Secure to soffit.

PROPRIETARY SILLS/ LINTELS/ COPINGS/ DRESSINGS

F30/720	SILLS, COPINGS AND DRESSINGS

-	See section H72.

F30/735	PRECAST CONCRETE LINTELS

-	To structural engineer’s specification.

F30/755	PREFABRICATED STEEL LINTELS

-	To structural engineer’s specification.

MISCELLANEOUS ITEMS

F30/810	CREASING TILES AT PARAPETS

-	Tiles: Plain clay to BS EN 1304.

-	Manufacturer: Contractor’s choice .

-	Placement: Two courses, broken jointed, true to line and level on full bed of 1:0.25:3 cement:lime:sand mortar as section Z21.

-	Joints: Full and finished flush.

F30/840	OPENINGS FOR FRAMES

-	Formation: Use accurate, rigid templates to required size.