C40	CLEANING MASONRY/ CONCRETE

To be read with Preliminaries/ General conditions.

GENERAL/ PREPARATION

C40/110	SCOPE OF WORK

-	Brickwork to first and secon floor north elevations (see drawings), but EXCLUDING elevations painted with murals.  Removal of atmospheric soiling, stains, deposits etc, using brushing and scraping, water spraying and plain poultices where necessary.

C40/120	RELATED REPAIR AND REMEDIAL WORKS

-	Work to be carried out before cleaning work: making good/pointing to cracks and joints .

C40/142	REMOVAL OF FITTINGS

-	Timing: Before commencement of cleaning work.

-	Disturbance to surfaces: Minimize.

-	Items for disposal: redundant pipework .

C40/160	PROTECTION

-	Surfaces not designated for cleaning: Prevent damage, including marking and staining.

-	Openings: Prevent ingress of water, cleaning agents, and detritus.

-	Vents and grilles: Seek instructions before sealing up.

-	Temporary mechanical fastenings:

-	In masonry: Locate in joints.

-	In other surfaces: Seek instructions.

C40/175	CONTROL AND DISPOSAL OF WASH WATER AND DETRITUS

-	Disposal: Safely. Obtain approvals from relevant Authority.

-	Control of wash water: Collect and divert to prevent ingress and damage to building fabric and adjacent areas.

-	Above and below ground drainage systems: Keep free from detritus and maintain normal operation.

C40/190	CLEANING GENERALLY

-	Operatives: Appropriately trained and experienced for each type of cleaning work.

-	Evidence of training: Submit on request.

-	Control of cleaning: Confine cleaning processes and materials to designated areas. Prevent wind drift.

-	Detritus: Remove regularly. Dispose of safely.

-	Monitoring: Frequently check results of cleaning compared to approved trial samples. If results established by trials are not achieved, seek instructions.

-	Modifications to cleaning methods and materials: Seek instructions.

C40/215	RECORD OF CLEANING WORKS

-	Written report: Record cleaning methods and procedures used for each type of surface and deposit.

-	Content: Relevant attributes of cleaning methods used including:

-	Equipment and settings.

-	Dwell times.

-	Number of applications.

-	Ambient temperatures.

-	Additional documentation: survey before cleaning .

-	Submission: At completion of cleaning works.

C40/230	TRIAL SAMPLES

-	Trial sample: .

-	Surface: brickwork .

-	Location/ Size: 2No, at low level, approx 1m x 1m .

-	Type of soiling: atmospheric soiling, stains, deposits etc.

-	Cleaning methods: brushing and scraping, water spraying, plain poultices.

-	Records: Maintain written records for each trial area, including cleaning methods and conditions, to enable replication of results elsewhere.

PRODUCTS/ EQUIPMENT

C40/332	WATER SPRAY (MOUNTED NOZZLES)

-	Equipment:

-	Spray/ Nozzle types: Atomising (nebulous).

-	Nozzles: Position and direction adjustable, relative to surfaces and profiles.

-	Controls: Time clock.

C40/372	PLAIN POULTICES FOR SALTS REMOVAL .

-	Poulticing medium manufacturer: Contractor’s choice .

-	Softening agent: Deionized water.

APPLICATION

C40/412	REMOVAL OF LOOSELY ADHERED DEPOSITS

-	Timing: Before commencement of other cleaning methods.

-	Surfaces: Prevent damage, including abrasion.

C40/432	TOOLING

-	Tooling of surfaces: Not permitted .

C40/462	WATER SPRAYED CLEANING (MOUNTED NOZZLES)

-	Surfaces: Minimize water run-off. Prevent damage.

-	Adjustment of washing cycle and nozzle positions: Regularly to achieve optimum cleaning performance.

C40/515	PLAIN POULTICING

-	Surfaces: Prevent damage, including abrasion.

-	Application: To wetted surfaces. Maintain contact with surfaces as poultice dries out.

-	Poultice reinforcement: submit proposals.

-	Drying: Prevent excessively rapid or localized drying out.

-	Spent poultice material: Do not reuse.