K11	RIGID SHEET FLOORING/ SHEATHING/ DECKING/ SARKING/ LININGS/ CASINGS

To be read with Preliminaries/ General conditions.

K11/436	WATER RESISTANT SHEATHING BOARD FOR TIMBER FRAMED WALLS

- Substrate: 50 x 150mm vertical timber studs at 600mm centres, as G20/210.

-	Additional supports: as clause 930.

- Support system: pre-treated timber battens, all site-cut ends to be liberally brushed with additional preservative.

-	Battens:

- Sizes: 50 x 50 mm.

-	Centres: max. 400 mm

-	Additional supports: as clause 930.

- Material: bitumen impregnated fibreboard with weatherproof coating on external face.

- Thickness 15mm

- Product reference: Hunton Bitroc

- Importer: Hunton Fibre (UK), tel. no. 01933 682683

- Distributor: Warren Insulation Ltd tel. no 01480 467972

-	Installation: Fix carefully and neatly to provide a complete barrier to water, snow and wind blown dust, in accordance with attached manufacturer’s technical information. All joints to be butted over studs and all edges to be fully supported.

- Fasteners: Galvanized, sherardized or stainless steel large head nails or stainless steel staples, in accordance with manufacturer’s technical information.

K11/515	PLYWOOD ROOF DECKING

-	Substrate: Joists as per Structural Engineer’s drgs + specification.

-	Additional supports: As per Structural Engineer’s drgs.

-	Decking: As G20/310A.

-	Type: WBP.

-	Grade: roofing.

-	Nominal thickness: 19mm .

-	Edges: Square.

-	Other requirements: N/A.

-	Setting out: Long edges running across supports. End joints central over joists and staggered.

-	Fixing:

-	Fasteners: 50 x 3.35mm galvanised annular ringed shank nails.

-	Fixing centres: Along each support: 25 mm from each long edge and at maximum 300mm centres between.

Around perimeter of roof area: Maximum 300mm centres.

-	Expansion provision: Clear expansion gap around perimeter of roof area and upstands: 10 mm.

- Intermediate expansion/ movement joints: As recommended by decking manufacturer.

K11/516	PLYWOOD FOR KERBS

-	Substrate: SW framing

-	Additional supports: As per Structural Engineer’s drgs.

-	Decking: Plywood manufactured to the relevant standards and quality control procedures specified in BS 5268-2, and so marked.

-	Type: WBP.

-	Grade: roofing.

-	Nominal thickness: 19mm .

-	Edges: Chamfered top edge, other edges square.

-	Other requirements: N/A.

-	Setting out: Long edges running across supports. End joints central over supports and staggered.

-	Fixing:

-	Fasteners: 50 x 3.35mm galvanised annular ringed shank nails.

-	Fixing centres: Along each support: 25 mm from each long edge and at maximum 150mm cc between.

K11/875	MEDIUM DENSITY FIBREBOARD FOR MISCELLANEOUS PIPWORK BOXINGS ETC

-	Substrate: timber battens .

-	Additional supports: as required .

-	Medium density fibreboard: To BS EN 622-5, Type moisture resistant .

-	Manufacturer/ Supplier: Contractor’s choice .

-	Thickness: 12mm .

-	Edges: square .

-	Fixing to supports:

-	Fasteners: As manufacturer’s recommendations .

-	Fixing centres (maximum): As manufacturer’s recommendations

Around board edges: As manufacturer’s recommendations .

Along intermediate supports: As manufacturer’s recommendations .

-	Fixing distance from edges (minimum): 12 mm.

WORKMANSHIP

K11/910	INSTALLATION GENERALLY

-	Timing: Building to be weathertight before fixing boards internally.

-	Moisture content of timber supports (maximum): 18%.

-	Joints between boards: Accurately aligned, of constant width and parallel to perimeter edges.

- Methods of fixing, and fasteners: As section Z20 where not specified otherwise.

K11/930	ADDITIONAL SUPPORTS

-	Additional studs, noggings/ dwangs (Scot) and battens:

-	Provision: In accordance with board manufacturer’s recommendations and as follows:

Tongue and groove jointed rigid board areas: To all unsupported perimeter edges.

Butt jointed rigid board areas: To all unsupported edges.

-	Size: Not less than 50 mm wide and of adequate thickness.

-	Quality of timber: As for adjacent timber supports.

-	Treatment (where required): As for adjacent timber supports.

K11/940	BOARD MOISTURE CONTENT AND CONDITIONING

-	Moisture content of boards at time of fixing: Appropriate to end use.

-	Conditioning regime: Submit proposals.

K11/960	FIXING GENERALLY

-	Boards/ sheets: Fixed securely to each support without distortion and true to line and level.

-	Fasteners: Evenly spaced in straight lines and, unless otherwise recommended by board manufacturer, in pairs across joints.

-	Distance from edge of board/ sheet: Sufficient to prevent damage.

-	Surplus adhesive: Removed as the work proceeds.

K11/980	OPEN JOINTS

-	Perimeter joints, expansion joints and joints between boards: Free from plaster, mortar droppings and other debris.

-	Temporary wedges and packings: Removed on completion of board fixing.

K11/990	ACCESS PANELS

-	Size and position: Agree before boards are fixed.

-	Additional noggings/ dwangs (Scot), battens, etc: Provide and fix as necessary.