J41	REINFORCED BITUMEN MEMBRANE ROOF COVERINGS

To be read with Preliminaries/ General conditions.

Section J41 deals with the installation of the Bauder Waterproofing System, comprising coverings of multiple layers of reinforced bituminous membranes laid and jointed using self-adhesive and/or torch application as required. It includes where required, the vapour control layer, thermal insulation, underlayer and capping sheet membranes (root resistant for green roof systems) and presumes the deck substrate and roof falls as stated within the specification below.  Accessories are included where relevant.

It is intended for use on projects where the detailed design is completed by the specifier (architect or landscape architect) with technical assistance from the manufacturer as required and should be read in conjunction with any project specific drawings provided.

SCOPE OF WORKS

This section includes:

- The Bauder waterproofing system.

- Thermal insulation to meet the clients required U value.

- Related Bauder system accessories (edge trims, linear drains etc).

This section does not include:

- Construction of the structural deck.

- Green Roof landscaping – refer section Q37-130A & Q37-130B.

- Cladding work – refer NBS Section H - Cladding / Covering

- Proprietary modular roof lights (supplied by others) - refer NBS section L10.

- Lead sheet coverings / flashings – See NBS Section H71.

- Fall arrest systems – refer NBS Section N25.

- Rainwater drainage systems - refer NBS Section R10.

TYPES OF COVERING

110A	BUILT-UP REINFORCED BITUMEN MEMBRANE WARM DECK ROOF COVERING

- Roof area: Roof Over G01-G04, G06, G07, G09, G15 & G17

- Substrate: New Plywood Deck (constructed to provide a roof slope of 2°).

-  Preparation: As clause 610A.

- Vapour control layer: Bauder VB4-Expal, 4 mm thick aluminium lined, elastomeric bitumen torch applied vapour barrier. Installation as clause 670D.

- Insulation: 120 mm thick, Bauder PIR Flatboard, fire resistant, zero ODP, highly efficient rigid urethane insulation.  Installation as clause 680C.

- Insulation to upstands: 30 mm thick, Bauder PIR Flatboard, fire resistant, zero ODP, highly efficient rigid urethane insulation.  Installation as clause 681A.

- Waterproof covering: BAUDER TOTAL GREEN ROOF SYSTEM

-  System Manufacturer: Bauder Limited, Broughton House, Broughton Road, Ipswich, Suffolk, IP1 3QR. Tel: 01473 257 671. Fax: 01473 230 761.

Email: technical@bauder.co.uk  Web: www.bauder.co.uk.

-  Underlayer: Bauder G4E, 4 mm thick, 200g/m² glass-fibre reinforced, elastomeric torch applied bitumen underlayer.

Attachment: As clauses 710, 740A.

-  Top layer / Cap sheet: Bauder Plant-E, 5 mm thick, 250g/m² polyester reinforced, elastomeric bitumen root resistant, torch applied capping sheet – green slate finish.

Attachment: As clauses 710, 750B.

- Flashings and detail work:

  - Bauder K5K capping sheet. Charcoal Grey finish. Install as clause 775B.

  - Form welted drip details to open perimeters serviced by external gutters, as clause 780A.

    - Surface protection: Extensive green roof landscaping - refer Section Q37-130A.

    - Accessories:  -

-     Bauder Insulation upstand support brackets.  Installation, as clause 775A.

  - Bauder 61 mm x 61 mm PIR angle fillets.  Installation, as clause 775A.

  - Bauder EM-Trim GRP edge trim – Profile type: as detail drawings.   Colour: to be agreed. Installation, as clause 785A.

- Additional Requirements: 210, 515, 520, 530, 540, 560, 561, 910B, 940.   Provision to be made (by others) for cutting a new chase to the existing rendered abutment, set a minimum of 150 mm above the finished surface of the new waterproofing, in preparation for new lead counter-flashing.

  - Provision for forming a chase and installing lead counter-flashings to rendered, brickwork or concrete upstands.  Refer Section H71, clauses 770, 780, 970.

110B	BUILT-UP REINFORCED BITUMEN MEMBRANE WARM DECK ROOF COVERING

- Roof area: Roof Over G20

- Substrate: New Plywood Deck (constructed to provide a roof slope of 3.5°).

-  Preparation: As clause 610A.

- Vapour control layer: Bauder VB4-Expal, 4 mm thick aluminium lined, elastomeric bitumen torch applied vapour barrier. Installation as clause 670D.

- Insulation: 120 mm thick, Bauder PIR Flatboard, fire resistant, zero ODP, highly efficient rigid urethane insulation.  Installation as clause 680C.

- Insulation to upstands: Insulation to upstands: 30 mm thick, Bauder PIR Flatboard, fire resistant, zero ODP, highly efficient rigid urethane insulation.  Installation as clause 681A.

- Waterproof covering: BAUDER TOTAL GREEN ROOF SYSTEM

-  System Manufacturer: Bauder Limited, Broughton House, Broughton Road, Ipswich, Suffolk, IP1 3QR. Tel: 01473 257 671. Fax: 01473 230 761.

Email: technical@bauder.co.uk  Web: www.bauder.co.uk.

-  Underlayer: Bauder G4E, 4 mm thick, 200g/m² glass-fibre reinforced, elastomeric torch applied bitumen underlayer.

Attachment: As clauses 710, 740A.

-  Top layer / Cap sheet: Bauder Plant-E, 5 mm thick, 250g/m² polyester reinforced, elastomeric bitumen root resistant, torch applied capping sheet – green slate finish.

Attachment: As clauses 710, 750B.

- Flashings and detail work:

  - Bauder K5K capping sheet. Charcoal Grey finish. Install as clause 775B.

  - Provision for forming a continuous gutter sole sheet liner in bauder K5K capping sheet.  Installation as clause 778.

    - Surface protection: Extensive green roof landscaping - refer Section Q37-130B.

    - Accessories:  -

-     Bauder Insulation upstand support brackets.  Installation, as clause 775A.

  - Bauder 61 mm x 61 mm PIR angle fillets.  Installation, as clause 775A.

- Additional Requirements: 210, 515, 520, 530, 540, 560, 561, 910B, 940.

Associated leadwork – refer Section H71.

  - Provision for forming a chase and installing lead counter-flashings to brickwork or concrete upstands (with no dpc present).  Refer H71, clause 770.

  - Site fabricated lead chute liners (supplied by others) to designated drainage positions, as per the clients requirements.  Refer Section H71, clause 810B.

  - Apply patination oil to all exposed areas of new lead subject to water run-off, as Section H71 clause 970.

130	BUILT-UP REINFORCED BITUMEN MEMBRANE COLD DECK ROOF COVERING

- Roof area: Roof Over G14.

- Substrate: New Plywood Deck (constructed to provide a roof slope of 2°).

-  Preparation: As clause 610A.

- Waterproof covering: BAUDER TOTAL GREEN ROOF SYSTEM

-  System Manufacturer: Bauder Limited, Broughton House, Broughton Road, Ipswich, Suffolk, IP1 3QR. Tel: 01473 257 671. Fax: 01473 230 761.

Email: technical@bauder.co.uk  Web: www.bauder.co.uk.

-  Underlayer: Bauder G4E, 4 mm thick, 200g/m² glass-fibre reinforced, elastomeric torch applied bitumen underlayer.

Attachment: As clauses710, 740A.

-  Top layer / Cap sheet: Bauder Plant-E, 5 mm thick, 250g/m² polyester reinforced, elastomeric bitumen root resistant, torch applied capping sheet – green slate finish.

Attachment: As clauses 710, 750B.

  - Flashings and detail work: -

  - Bauder K5K capping sheet. Charcoal Grey finish. Install as clause 775B.

  - Provision for forming a continuous gutter sole sheet liner in bauder K5K capping sheet.  Installation as clause 778.

- Surface protection: Extensive green roof landscaping - refer Section Q37-130A.

- Accessories: -

  - Bauder EM-Trim GRP edge trim – Profile type: as drawings. Colour: to be agreed. Installation, as clause 785A.

  - AIRTRAK – AB Abutment Ventilator, fixed in accordance with manufacturer’s recommendations.

- Additional Requirements: 210, 515, 520, 530, 560, 561, 910B, 940.

Associated leadwork – refer Section H71.

  - Provision for forming a chase and installing lead counter-flashings to brickwork or concrete upstands (with no dpc present).  Refer H71, clause 770.

  - Site fabricated lead chute liners (supplied by others) to designated drainage positions, as per the clients requirements.  Refer Section H71, clause 810B.

  - Apply patination oil to all exposed areas of new lead subject to water run-off, as Section H71 clause 970.

PERFORMANCE

J41/210	ROOF PERFORMANCE

- General: Secure, free draining and weather tight.

PRODUCTS

J41/320A		FAST DRYING PRIMER

- Type: Any commercially available fast drying Bituminous Priming Solution meeting characteristics of BS 8217, clause 5.6.2., supplied by an approved installer.

J41/325	BONDING COMPOUND

- Type: Oxidized bitumen to BS 3690-2, grade 95/25.

- Restriction: For heat sensitive insulation materials, use cold bonding compounds.

J41/330	TIMBER TRIMS, ETC

- Quality: Planed. Free from wane, pitch pockets, decay and insect attack (except ambrosia beetle damage).

- Moisture content at time of covering (maximum): 22%.

- Preservative treatment: Please note organic solvent based timber preservatives are not permitted, as these attack bitumen based materials.

EXECUTION GENERALLY

J41/515	ADVERSE WEATHER

- General: Do not lay coverings in high winds, wet or damp conditions or in extremes of temperature unless effective temporary cover is provided over working area.

- Unfinished areas of roof: Keep dry, protect edges of laid membrane from wind action.

J41/520	INCOMPLETE WORK

- End of working day: Provide temporary seal to prevent water infiltration.

- On resumption of work: Cut away tail of membrane from completed area and remove from roof.

J41/530	APPLYING PRIMERS

- Coverage per coat (minimum): As per manufacturer’s recommendations.

- Surface coverage: Even and full.

- Coats: Fully bond. Allow volatiles to dry off thoroughly between coats.

J41/540	APPLYING BONDING COMPOUNDS

- Roof sited boilers: Not permitted

- Temperature of compound: Suitable to achieve bond over whole surface. Do not overheat.

560	GENERAL WORKMANSHIP REQUIREMENTS

- Installation of the Bauder waterproofing system may only be carried out by trained and certified operatives approved by Bauder Ltd and who carry current ID badges. These should be available for inspection at all times.

- Workmanship must comply with Codes of Practice BS 8217:2005 (or alternatively Bauder Ltd’s specification where otherwise stated).  Non-compliant workmanship will not be permitted, even if the system is watertight.  The client will be told that all such faults must be remedied, before the Guarantee is issued.

- All waterproofing materials and system components must be supplied by Bauder Ltd, unless otherwise stated.  Any sub-standard materials or un-authorised alternatives will be rejected.  Any building work which is the responsibility of the roofing contractor and has a bearing on the life of the Bauder System must be carried out by properly trained and qualified tradesmen.

- Any structural damage, peculiarities or details discovered that might affect the performance of the Bauder system, should be reported immediately to the client’s representative and Bauder Limited in order that they may assist in overcoming the problem.

- The contractor is to ensure water tightness of the roof at all times.  Proper day joints must be formed at the end of each working day to provide a temporary seal.  No mopping or loose covers will be permitted.

- Where building works are to be carried out by other trades, following completion of the waterproofing, the contractor must make adequate provision for supplying protection to prevent damage to the new membranes. The final inspection will not be carried out by the independent surveyor until all associated trades are complete and the roof areas are clear from all debris and protection layers.

- All mechanical and electrical work to plant and equipment should be carried out by competent mechanical and electrical qualified tradesmen.  All plant is to be reinstated and re-commissioned on completion of the roofing works in accordance with the client's detailed specification.

- Where building works are to be carried out by other trades, following completion of the waterproofing, the contractor must make adequate provision for supplying protection to prevent damage to the new waterproofing.

- If any items of plant/equipment are to be situated on the finished roof, a sacrificial layer of Bauder capping sheet is to be loose laid beneath.  This is to extend a minimum 25mm past the point of contact on all sides.  In the case of heavy items it may be necessary to introduce a load-spreading slab, please contact Bauder for further advice.

- All lead work to be carried out by skilled tradesmen and in accordance with current codes of practise and the recommendations of the Lead Development Association.

- All lead work to be carried out by skilled tradesmen and in accordance with current codes of practise and the recommendations of the Lead Development Association.

561	SITE INSPECTIONS

- Bauder Site technicans will carry out regular inspections of the project during the course of the works.  The Approved Contractor must give reasonable notice to Bauder of their intention to commence laying capping sheet.  This will allow a discretionary inspection of the underlayer to take place, so that any remedial treatment necessary can be carried out prior to installing the capping sheet.  This is particularly important when tapered insulation has been used to ensure that any areas of ponding water that may remain can be addressed.

- Bauder must be notified when the roof is ready for final inspection and all related works and snagging complete.  See also clauses 910A or 910B (Landscaped roofs).

SUBSTRATES / VAPOUR CONTROL LAYERS / WARM ROOF INSULATION

J41/610A	SUITABILITY OF SUBSTRATES (PLYWOOD)

- Substrates generally: Secure, clean, dry, smooth, free from frost, contaminants, voids and protrusions.  The new 18 mm thick WPB plywood should be BBA certified, conforming to BS5268 Part 2:2002 & CPD/CE compliant, fixed directly to either the joists or firings using non corroding ring shank nails or recommended screw fasteners.

- Falls: Where provided, the falls/cross-falls should be designed to 1:40 to achieve minimum finished falls of 1:60.  No deflections or back-falls present if the deck is designed to achieve a 0° level finished surface (e.g. when using tapered insulation to provide falls).

- Preliminary work: Complete including:

-  Formation of upstands, kerbs, box gutters, sumps, grooves, chases and expansion joints.

-  Fixing of battens, fillets and anchoring plugs/strips.

- Moisture content and stability of substrate: Must not impair roof integrity.

- Preparation: All such items to be rectified as necessary to eliminate the possibility of puncturing the new waterproofing system.

- Taping of board joints: Tape centrally over board joints with 200mm wide strips of Bauder R333 taping strip. These can be retained temporarily in place with clout nails, prior to the self adhesive vapour barrier being laid.

- Priming: Prime all areas receiving the new waterproofing with fast drying bitumen primer, as clause 320A, and ensure this is thoroughly dry before applying the new waterproofing.

J41/640	FIXING TIMBER TRIMS

- Fasteners: type/length appropriate and suitable to particular deck substrate.

- Fixing centres (maximum): 500 mm.

J41/670D	LAYING VAPOUR CONTROL LAYER

- Attachment: Fully bonded to deck substrate in accordance with manufacturer’s requirements.

- Side and end laps: minimum 100 mm, with all laps torch sealed to provide a 5-10 mm bitumen bead extrusion.  Installation methods as recommended by manufacturer.

- Penetrations: Fully seal using bonding methods recommended by manufacturer.

- Edges of insulation at roof edges, abutments, upstands, kerbs, penetrations and the like: Enclose, with vapour control layer:

-  Dressed up 150 mm above surface of insulation, thus providing 100 mm (minimum) seal when overlapped by the roof covering.

J41/680C	LAYING WARM ROOF INSULATION

- Setting out:

-  Long edges: Fully supported

-  End edges: Fully supported.

-  Joints: close butted together.

-  End joints: Stagger.

- Bedding: Fully bond to vapour control layer in hot bitumen, as clauses 325 & 540. The board surface with the Bauder logo printed on, must be laid face upwards.

- Multiple board layers: Where the total thickness of insulation required is greater than can be achieved by a single standard board, then additional boards of the same product can be adhered to make up the total thickness required.  These additional boards should be fully bonded using 95/25 grade hot bitumen compound.

- Bauder Perimeter Insulation facing strip: Apply a 500 mm wide strip of self-adhesive, 2 mm thick, BauderTEC KSA Sprint DUO to the surface of the insulation boards at all perimeter edges, rainwater outlets, rooflights, vent pipes, penetrations and any other similar abutments, to create a full bonding zone once the underlayer is applied. The self-adhesive membrane is cold applied by removing the peel off release film and smoothing into place.  Adjacent lengths of strip to be close butted. Where insulated upstands are present, this membrane can also be used to secure the angle fillet into position.  Care must be taken to avoid creating water checks, especially around rainwater outlets, chutes and gutters.

- Protection to exposed edges of insulation: Reduced thickness treated timber batten as clause 640 (or equivalent plywood construction), a minimum width of 150 mm and 10 mm less in thickness than the insulation to accommodate the build-up of the waterproofing layers – all securely fixed to the deck. Outer edges chamfered at changes in level.

- Completion: Boards must be in good condition, well fitting and stable.

681A	INSTALLING WARM ROOF INSULATION (INSULATED UPSTANDS)

- Bedding: Fully bonded to the vapour control layer using hot bitumen compound, as clauses   325 and 540.  Board joints to be close butted.

- Protective hard edges: treated timber battens or Bauder Insulated upstand brackets (as appropriate to given detail situation) must be used at all right angled edges e.g. top edges of parapet walls or abutment upstands.

- Encapsulation seal: Provision must be allowed for forming a minimum 100 mm lap seal between the vapour control layer and underlayer, where the insulation finishes.

WATERPROOF COVERINGS/ ACCESSORIES

J41/710		LAYING REINFORCED BITUMEN MEMBRANES GENERALLY

- Direction of laying: Unrolled up the slope.

-  Where practicable, install so that water drains over and not into laps.

- Side and end laps (minimum): 100 mm, with the exception of mineral surfaced membranes, where side laps are 80 mm, but the head laps to remain 100 mm.

- Head and side laps: Offset.

- Intermediate and top layer/Capping sheet: Fully bond.

- Successive layers: Apply without delay. Do not trap moisture.

- Strips of bitumen membrane for 'linear' details: Cut from length of roll e.g. gutter sole pieces.

- Detail flashings: to be cut from width of roll.

- Completed coverings: Firmly attached, fully sealed, smooth, weather proof and free draining.

J41/740A		TORCH-ON BONDING OF REINFORCED BITUMEN UNDERLAYER

- Bond: Partially bonded in the approved Bauder manner.

- Laps: Head and side laps to be 100 mm. All laps to upstands, edge details, flashings, etc., to be a minimum 100 mm.  The underlayer must be taken up all upstands, edge details, in accordance with current British Standards and the manufacturer’s recommendations.

- Underlayer inspection: The Approved Contractor must give reasonable notice to the nominated Bauder Site Technician of their intention to commence laying capping sheet.  This will allow a discretionary inspection of the underlayer to take place, so that any remedial treatment necessary can be carried out prior to installing the capping sheet.

750BJ41/	LAYING REINFORCED BITUMEN TORCH-ON CAPPING SHEET

- Bond: Full over whole surface, with no air pockets.

- Excess compound at laps of top layer/ capping sheet: Leave as a 5 mm - 10 mm continuous bitumen bead extrusion.

- Laying top layer: Fully bonded to the underlayer by torching in the approved Bauder manner. Head laps to be 100 mm, side laps to be 80 mm. All laps to upstands, edge details, flashings, etc. to be 100 mm.

- Final Inspection: No landscaping is to be applied until the root resistant capping sheet has been thoroughly inspected by the Bauder Site Technician. This is to ensure that any remedial treatment that is necessary can be carried out prior to laying the landscaping elements.  Failure to ensure the instigation of this inspection will result in the issuing of the Bauder guarantee being put in jeopardy.

J41/775A		SKIRTINGS AND UPSTANDS

- Insulated upstand brackets: At all abutment upstands, Bauder insulated upstand support brackets must be used.  These are to be fixed at 400mm centres using suitable fixings through the vapour barrier, so that the top edge is a minimum of 300mm above the surface of the deck.  A 3mm gap should be left between adjacent sections.  The detail is to be carried out in accordance with the Bauder detail drawing, where provided.

- Angle fillets: Bauder PIR angle Fillets (61 mm x 61 mm) must be used at all right angled upstands, provisionally bonded in Bauder PUR membrane adhesive and subsequently retained once the underlay detailing is applied..  Under no circumstances must fillets of an alternative material be incorporated (i.e. cork, fibre, etc.) as this would invalidate the guarantee.

- Layers of bitumen membrane: Carry in staggered formation up upstand, with each layer fully bonded.

- Upstands:

- At ends of rolls: Underlay layer only, form with bitumen membrane carried up without using separate strip.

- Elsewhere: Form with matching strips of bitumen membrane, maintaining laps.

- Additional fixing of bitumen membranes: Mechanically fix the top leading edge of all upstand details in excess of 250 mm in height using appropriate fasteners.  In the event of doubt, Bauder should be consulted regarding any specific requirement.

- Upstand details (minimum height): 150 mm.  This must be taken from the surface of the finished landscaping. Special attention should be paid to all structures, such as rooflights, counter-flashings, window and door cills, pipes etc. Bauder cannot take responsibility for water ingress over waterproofing details constructed below the recommended minimum height.

- Flashings: Separate flashings must always be formed. Capping sheet taken up the upstand in one piece will not be permitted.

J41/775B		SKIRTINGS AND UPSTANDS

- Angle fillets: as per clause 335A, must be incorporated at all right angled upstand abutments, screw fixed to the structural deck. Alternatively, BauderPIR angle fillets may be used, bonded using cold applied Bauder polyurethane membrane adhesive.  Under no circumstances must fillets of an alternative material be incorporated (i.e. cork, fibre, etc.) as this would invalidate the guarantee.

- Layers of bitumen membrane: Carry in staggered formation up upstand, with each layer fully bonded.

- Upstands: -

At ends of rolls: Underlay layer only - Form with specified bitumen membrane carried up without using separate strip.

- Elsewhere: Form with matching strips of bitumen membrane, maintaining laps.

- Additional fixing of bitumen membranes: Mechanically fix all upstands in excess of 250 mm in height using appropriate fasteners.  In the event of doubt, Bauder should be consulted regarding any specific requirement.

- Upstand details (minimum height): 150 mm minimum, taken from the surface of the finished landscaping. Special attention should be paid to all structures, such as rooflights, counter-flashings, window and door cills, pipes etc. Bauder cannot take responsibility for water ingress over waterproofing details constructed below the recommended minimum height.

- Flashings: Separate flashings must always be formed. Capping sheet taken up the upstand in one piece will not be permitted.

778	CONTINUOUS GUTTER SOLE SHEET

- Supply and fix a layer of Bauder capping sheet so as to run lengthways along the gutter detail forming a continuous sole sheet, so as to minimise laps and water checks.  All adjacent cap sheet detail waterproofing is to be dressed down into the gutter channel and bonded onto the sole sheet.

J41/780A		WELTED DRIPS

- Material: Bauder K5K

-	Length: Form using maximum width strips.

-	Height at external gutter (minimum): 75 mm.

- Welt tail: Nail to face of drip batten. Fold neatly.

- Welt: Bond together, carry minimum 150 mm onto roof. Overlap with bitumen membrane capping sheet.

J41/785A		FIXING PERIMETER TRIMS

- First / Intermediate layers bitumen membrane: Lay over roof edge upstand. Project free edge 25 mm from wall or fascia.

- Trim:

-	Setting out: 3 mm (minimum) clear from wall or fascia.

-	Fasteners: Screw fasteners of type appropriate to kerb or deck substrate. Nail fixing is not permitted.

-	Fixing: 30 mm from ends and at 300 mm (maximum) centres.

-	Jointing sleeves / bridging piece: must be provided to each joint.

-	Corner pieces: Purpose made.

- Completion:

-	Contact surfaces: Prime.

-	Joints: Cover with 150 mm long pads of bitumen membrane, bonded to trim.

- Completion of bitumen membrane:

-	Top layer/ Capping sheet: Butt joint to rear edge of trim.

-	Cover strip: Fully bond to trim and top layer/ capping sheet of bitumen membrane. Carry over roof edge upstand and lap 100 mm onto roof. The capping sheet is to be dressed tightly into the top lip of the trim, ensuring a bead of bitumen extrudes at the edge.

- Wall / kerb joints: The new trim must cover any open joint that may exist at the top of the kerb or wall, by a minimum distance of 20mm.

- Cover strip material: Bauder K5K

COMPLETION

J41/910B		INSPECTION

- Interim and final roof inspections: in accordance with the manufacturer’s requirements for guarantee.

- Notification: It is the responsibility of the approved contractor to advise Bauder Ltd when the roof is ready for Final Inspection.  The ‘Final Inspection’ of the waterproofing must be carried out and approved by Bauder Ltd prior to any landscaping products/materials being installed, otherwise a guarantee cannot be issued.

- Other requirements: Please also refer to preliminaries / general conditions.