F31	PRECAST CONCRETE SILLS/ LINTELS/ COPINGS/ FEATURES

To be read with Preliminaries/ General conditions.

TYPES OF COMPONENT

F31/140	CONCEALED PRECAST LINTELS

-	Concrete: Designated to BS 8500-2: Minimum RC30.

-	Aggregate size (maximum): 20 mm.

-	Reinforcement provision for spans up to 1800 mm:

Clear span		Section	Bearing	Reinforcement

________________________________________________

Up to		140 mm deep	150 mm at	One 2 mm

900 mm		x width of	both ends	mild steel bar for

wall		for each 	105 mm of wall thickness.

________________________________________________

900 to 		215 mm deep	225 mm at	One 16 mm

1800 mm		x width of	both ends	mild steel bar for

wall		for each 	105 mm of wall thickness.

________________________________________________

-	Cover to reinforcement: 20 mm minimum.

F31/150	CONCRETE PRECAST THRESHOLDS  AND CILLS TO EXTERNAL DOORS AND WG18C, SEE DETAILS

-	Concrete: Designated to BS 8500-2: Minimum RC30.

-	Aggregate size (maximum): 20 mm.

-	Other requirements: Smooth visible faces.

.

GENERAL REQUIREMENTS

F31/210	MOULDS

-	Permissible fabrication and operating tolerances: Length 0 to +6 mm, other dimensions ±3 mm.

F31/220	CONCRETE GENERALLY

-	Specification: To  BS 8500-2 and BS EN 206-1.

-	Producer: Currently certified by a body accredited by UKAS to BS EN 45011 for product conformity certification of ready-mixed concrete.

-	Chloride class of concrete: Excluding SPRC: C 10.40

-	Using SRPC: C1 0.20.

-	Reinforced and heat cured: C1 0.10.

-	Prestressed: C1 0.10.

-	Admixtures containing calcium chloride: Not allowed.

F31/250	REINFORCEMENT

-	Carbon steel reinforcement: As appropriate to BS 4449,

BS 4482 and BS 4483.

-	Cutting and bending: To BS 8666.

-	Galvanized reinforcement: Galvanized to BS EN ISO 1461 after cutting. Chromate treated.

-	Stainless steel reinforcement: To BS 6744.

-	Designation: 1.4301.

-	Cutting and bending: To BS 8666.

-	Non structural reinforcement: Include to resist shrinkage and handling stresses.

-	Bimetallic corrosion and staining: Prevent by appropriate selection and use of materials.

-	Condition at time of placement: Clean, free of corrosive pitting, loose materials and substances that adversely affect reinforcement, concrete, or bond between the two.

-	Fixing: Accurate and secure.

-	Method: Wire tying, approved steel clips or tack welding if permitted.

-	Concrete cover: Maintain free of all tying wire or clips.

F31/260	CASTING AND CURING

-	Placing of concrete: Thoroughly compact.

-	Protection against drying out: Methods and duration to

BS EN 13369 clause 4.2.1.3.

-	Immature components: Avoid movement, vibration, overloading, physical shock, rapid cooling and thermal shock.

-	Delivery to site: Not until at least 14 days after casting.

FAIR FACED COMPONENTS

F31/330	MIXES FOR VISIBLE FACED COMPONENTS

-	Constituent materials and mix design for each finish type: To remain constant.

-	Colour and appearance of each finish type: To remain constant.

-	Aggregates: To BS EN 12620.

-	Origin: Single source for each finish type, having sufficient quantity for whole contract.

F31/341	CONDITIONS FOR SEPARATE FACING AND BACKING MIXES

-	Difference in cement content: Not greater than 80 kg/m3.

-	Thickness of facing mix: 10 mm greater than maximum aggregate size, minimum 25 mm.

-	Location of reinforcement: Minimum 20 mm away from the interface between mixes.

-	Compaction of facing and backing mix: Carry out to create monolithic construction.

F31/350	QUALITY OF FINISHES

-	Appearance standard: As established by samples.

F31/370	COVER ON VISIBLE FACES

-	Spacers: Not permitted.

-	Proposed method statement: Submit.

F31/380	CONSISTENCY OF PRODUCTION METHODS

-	Production methods: To remain consistent for each matching type of finish.

-	Finish appearance: To remain within the range of variation indicated by the samples submitted.

-	Changes to production methods: If variations are proposed for components of the same finish, submit evidence that there will be no difference in appearance.

INSTALLATION

F31/420	LAYING

-	Mortar for bedding and jointing: As section Z21.

-	Mix: 1:1:6 .

-	Packing: If required use slate.

-	Bedding components: On full bed of mortar

-	Removal of marks, stains and extraneous mortar on visible faces: Rubbing not permitted.

F31/430	SUPPORT OF EXISTING WORK OVER NEW LINTELS

-	Joint above lintels: Fully fill and compact with semidry mortar.

F31/440	ONE PIECE SILLS/ THRESHOLDS

-	Bed joints: Leave clear of mortar except at end bearings and beneath masonry mullions.

-	On completion: Point with mortar to match adjacent work.