P10	SUNDRY INSULATION/ PROOFING WORK

To be read with Preliminaries/ General conditions.

TYPES OF INSULATION

P10/140	INSULATION FITTED BETWEEN RAFTERS

-	Material: Mineral wool .

-	Standard: T0 BS EN 13162 .

-	Manufacturer: Rockwool .

-	Product reference: Rickwool Roll .

-	Thickness: 150mm .

-	Installation requirements:

-	Joints: Butted, no gaps.

-	Fasteners: Used where necessary to retain insulation and/ or prevent slumping.

-	Air space above insulation: Not restricted.

-	Eaves ventilation: Unobstructed.

P10/210	INSULATION FITTED BETWEEN 150 MM THICK STUDS

-	Material: Mineral wool

-	Manufacturer: Rockwool Ltd

Tel: 01656 862621

Fax: 0871 222 1784

E-mail: info@rockwool.co.uk

-	Product reference: Flexi

-	Thickness: 140 mm

-	Installation requirements:

-	Joints: Butted, no gaps.

- Fasteners: Used to prevent slumping/ displacement.

P10/211	INSULATION FITTED BETWEEN 50 MM THICK BATTENS & AROUND INTERNAL BOXED IN SOIL PIPES AND RAINWATER PIPES

-	Material: Mineral wool

-	Manufacturer: Rockwool Ltd

Tel: 01656 862621

Fax: 0871 222 1784

E-mail: info@rockwool.co.uk

-	Product reference: Flexi

-	Thickness: 50 mm

-	Installation requirements:

-	Joints: Butted, no gaps.

- Fasteners: Used to prevent slumping/ displacement.

P10/310	VAPOUR CONTROL LAYER FIXED TO TIMBER STUDS/ JOISTS/ FRAMING

-	Material: 1000 gauge virgin polyethylene.

-	Manufacturer: Contractor’s choice to PIFA Standard 6/83A or Agrément certified.

-	Minimum vapour resistance: 250MN s/g.

-	Moisture content of timber at time of fixing (maximum): 20%.

-	Installation requirements:

-	Set out: With continuity, minimum joints.

-	Method of fixing: Secure with staples at not more than 250 mm centres along all supports. No sagging.

-	Lapped joints: At supports only, 150 mm minimum.

-	Openings: Lap over and fix to reveals.

-	Joints and edges: Sealed with double sided tape with vapour resistivity not less than the vapour control layer.

-	Penetrations: Sealed.