# Q25 Slab/ brick/ sett/ cobble pavings

To be read with Preliminaries/ General conditions.

GENERAL

120	CONCRETE FLAG PAVING SYSTEM TO ALL EXTERNAL STEPS AND TO RAMP ON EAST ELEVATION

•	 Granular sub-base: Highways Agency Type 1 granular material, as section Q20.

- Thickness: 150 mm.

•	 Base: Concrete as section Q21.

- Thickness: 75 mm.

•	 Laying course: Site mixed mortar.

- Accessories: None.

•	 Paving units: Marshalls Perfecta paving slabs, step treads and risers (with rubber

compound visibilty strips) and Marshalls tactile paving.

•	 Jointing: Site mixed mortar.

- Bond: Straight line.

•	 Accessories: None.

130	RIGID BRICK PAVING SYSTEM FLUSH BORDERS TO BITMAC, RESIN BOUND

PERMEABLE PAVING AND SOFT PLAY SURFACE

•	 Granular sub-base: Highways Agency Type 1 granular material, as section Q20.

-	Thickness: 150 mm.

•	 Concrete base: Concrete as section Q21.

-	Thickness: 75mm.

•	 Paving units: facing bricks to match elsewhere.

•	 Bedding and jointing: Site mixed mortar.

-	Bond: Stack bond BOE.

•	 Movement joints: not applicable.

-	Locations: not applicable.

•	 Accessories: None.

160	NATURAL STONE COBBLE PAVING SYSTEMSAFETY STRIP ADJACENT TO FRONT ELEVATION WINDOWS

•	 Granular sub-base: Highways Agency Type 1 granular material, as section Q20.

-	Thickness: 150 mm.

•	 Base: Concrete as section Q21.

-	Thickness: 75 mm.

•	 Paving units: Selected hard smooth, egg-shaped kidney flint cobbles, laid long end

upwards in close random pattern.

•	 Laying course and jointing: Site mixed class II mortar.

•	 Overall nominal thickness of cobbles and bedding: 150 mm.

PRODUCTS

370	CEMENT FOR SITE MIXED MORTAR FOR BRICK EDGES, COBBLES AND

CONCRETE PAVING

•	 Standard: As section Z21.

435	PRIMER FOR UNDERSIDE OF FLAGS AND SLABSIF RECOMMENDED BY

MARSHALLS

•	 Manufacturer: Contractor's choice.

-	Product reference: Contractor's choice.

EXECUTION

620	ADVERSE WEATHER

•	 General:

- Temperature: Do not lay or joint paving if the temperature is below 3° on a

falling thermometer or below 1° on a rising thermometer.

- Frozen materials: Do not use. Do not lay bedding on frozen or frost covered

bases.

•	 Paving with mortar joints and/ or bedding:

- Protect from frost damage, rapid drying out and saturation until mortar has

hardened.

•	 Paving laid and jointed in sand:

-	Stockpiled bedding sand: Protect from saturation.

-	Exposed areas of sand bedding and uncompacted areas of sand bedded

paving: Protect from heavy rainfall.

- Saturated sand bedding: Remove and replace, or allow to dry before

proceeding.

-	Laying dry-sand jointed paving in damp conditions: Brush in as much jointing

sand as possible. Minimize site traffic over paving. As soon as paving is dry,

top up joints and complete compaction.

625	LAYING PAVINGS - GENERAL

•	 Appearance: Smooth and even with regular joints and accurate to line, level and

profile.

•	 Falls: To prevent ponding.

•	 Bedding of paving units: Firm so that rocking or subsidence does not occur or

develop.

- Bedding/ Laying course: Consistently and accurately graded, spread and

compacted to produce uniform thickness and support for paving units.

•	 Slopes: Lay paving units upwards from the bottom of slopes.

•	 Paving units: Free of mortar and sand stains.

•	 Cutting: Cut units cleanly and accurately, without spalling, to give neat junctions with

edgings and adjoining finishes.

630	LEVELS OF PAVING

•	 Permissible deviation from specified levels:

-	Generally: ± mm.

•	 Height of finished paving above features:

-	At gullies: +6 to +10 mm.

-	At drainage channels and kerbs: +3 to +6 mm.

635	REGULARITY

•	 Maximum variation in gap under a 3 m straight edge placed anywhere on the surface

(where appropriate in relation to the geometry of the surface): 10 mm.

•	 Sudden irregularities: Not permitted.

•	 Difference in level between adjacent blocks/ pavers/ setts (maximum): 2 mm.

645	PROTECTION

•	 Cleanliness: Keep paving clean and free from mortar droppings, oil and other materials likely to cause staining.

•	 Materials storage: Do not overload pavings with stacks of materials.

•	 Handling: Do not damage paving unit corners, arrises, or previously laid paving.

•	 Mortar bedded pavings: Keep free from traffic after laying:

-	Pedestrian traffic (minimum): 4 days.

-	Vehicular traffic (minimum): not permitted.

•	 Access: Restrict access to paved areas to prevent damage from site traffic and plant.

650	CEMENTITIOUS BASES AND SUB-BASES

•	 General: Protect from moisture loss, if not covered by another pavement course

within 2 hours of completion.

655	CONDITION OF SUB-BASES/ BASES BEFORE SPREADING LAYING COURSE

•	 Trenches and excavation of soft or loose spots in subgrade: Fill and thoroughly

compact.

•	 Granular surfaces: Lay and compact so as to be sound, clean, smooth and close-

textured enough to prevent migration of bedding/ laying course materials into the sub-

base during compaction and use, free from movement under compaction plant and free

from compaction ridges, cracks and loose material.

•	 Prepared existing and new bound bases (roadbases): Sound, clean, free from rutting

or major cracking. Remove sharp stones, projections and debris.

•	 Sub-base/ Roadbase level tolerances: To BS 7533-7, Annex A.

•	 Levels and falls: Accurate and within the specified tolerances.

•	 Drainage outlets: Within 0-10 mm of the required finished level.

•	 Features in sand bedded paving (including mortar bedded restraints and drainage

ironwork): Complete to required levels; adequately bed and haunch in mortar.

•	 Sub-bases containing cement/ hydraulic binder: Cure for minimum times specified in

BS 7533-4.

695	SITE MIXED MORTAR - LAYING COURSE FOR BRICK EDGINGS AND COBBLES

•	 Mix: 1:0.25:3 cement:lime:sand.

•	 Consistency: Stiff plastic.

•	 Admixtures: TBA.

715	LAYING FLAG AND SLAB PAVING - MORTAR LAYING COURSE AND JOINTING

•	 Standard generally: In accordance with BS 7533-4.

•	 Flag installation and cutting: To Interpave 'Concrete flag paving'.

•	 Laying course:

-	Nominal thickness: 25 mm after compaction.

•	 Laying and jointing: To Marshalls recommendations.

•	 Joint width (nominal): 5-10 mm.

725	LAYING RIGID BRICK PAVING

•	 Standard generally: In accordance with Brick Development Association Design Note

8.

•	 Bedding and jointing method: Simultaneous bedding and jointing with stiff plastic

mortar.

•	 Cement slurry: Apply thin slurry (1-3 mm) of neat cement or 1:1 cement:soft sand

over the freshly laid mortar bed immediately prior to laying bricks.

•	 Laying: Wet bricks as necessary (but do not soak), butter joint faces and press down

firmly to give a level surface with 10 mm regular joints.

•	 Nominal thickness of bed: 25-30 mm.

•	 Joint profile: Flush.

750	LAYING NATURAL STONE COBBLE PAVING

•	 Bedding, laying, jointing and completion: In accordance with BS 7533-7 and -10.