M50	RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING

To be read with Preliminaries/ General conditions

TYPES OF COVERING

M50/150	SHEETING - LINOLEUM

-	Location: Flooring in new and existing areas, where shown on drawings

-	Base: Screed

-	Preparation: To manufacturer’s recommendations

-	Fabricated underlay: Not required

-	Flooring roll: To BS EN 548

- Manufacturer: ForboNairn Ltd

    - Tel: 01592 643777

    - Fax:01592 643999

    - E-mail: info.uk@forbo.com

Product reference: Marmoleum

-	BS EN 685 class: A

-	Width: 2000 mm

-	Thickness: 2.5 mm

-	Colour/ pattern: To be approved

-	Adhesive (and primer if recommended by manufacturer): To manufacturer’s recommendations

-	Seam welding: To manufacturer’s recommendations

-	Accessories: Edgings/Cover strips as clause 740. Coved skirting as clause 770

-	Finishing: To manufacturer’s recommendations

-	Other requirements: Not required

GENERAL REQUIREMENTS

M50/210	WORKMANSHIP GENERALLY

-	Base condition after preparation: Rigid, dry, sound, smooth and free from grease, dirt and other contaminants.

-	Finished coverings: Accurately fitted, tightly jointed, securely bonded, smooth and free from air bubbles, rippling, adhesive marks and stains.

M50/250	LAYOUT – ROLL MATERIALS

-	Setting out of seams: Before placing orders agree setting out for sheeting types M50/ M50/150

M50/330	COMMENCEMENT

-	Required condition of works prior to laying materials:

-	Building is weathertight and well dried out.

-	Wet trades have finished work.

-	Paintwork is finished and dry.

-	Conflicting overhead work is complete.

-	Floor service outlets, duct covers and other fixtures around which materials are to be cut are fixed.

-	Notification: Submit not less than 48 hours before commencing laying.

M50/340	CONDITIONING

-	Prior to laying: Condition materials by unpacking and separating in spaces where they are to be laid. Maintain resilient flooring rolls in an upright position. Unroll carpet and keep flat on a supporting surface.

-	Conditioning time and temperature (minimum): As recommended by manufacturer with time extended by a factor of two for materials stored or transported at a temperature of less than 10°C immediately prior to laying.

M50/350	ENVIRONMENT

-	Temperature and humidity: Before, during and after laying, maintain approximately at levels which will prevail after building is occupied.

-	Ventilation: Before during and after laying, maintain adequate provision.

M50/360	FLOORS WITH UNDERFLOOR HEATING

-	Commencement of laying: Not before a period of 48 hours after heating has been turned off.

-	Post laying start up of heating system: Slowly return heating to its operative temperature not less than 48 hours after completing laying.

PREPARING BASES

M50/410	NEW BASES

-	Suitability of bases and conditions within any area:

Commencement of laying of coverings will be taken as acceptance of suitability.

M50/420	EXISTING BASES

-	Notification: Before commencing work, confirm that existing bases will, after preparation, be suitable to receive coverings.

-	Suitability of bases and conditions within any area:

Commencement of laying of coverings will be taken as acceptance of suitability.

M50/430	NEW WET LAID BASES

-	Base drying aids: Not used for at least four days prior to moisture content testing.

-	Base moisture content test: Carry out in accordance with BS 5325, Annexe A or BS 8203, Annexe A.

-	Locations for readings: In all corners, along edges, and at various points over area being tested.

-	Commencement of laying coverings: Not until all readings show 75% relative humidity or less.

M50/440	SUBSTRATES TO RECEIVE THIN COVERINGS

-	Trowelled finishes: Uniform, smooth surface free from trowel marks and other blemishes. Abrade suitably to receive specified floor covering material.

M50/460	SMOOTHING/ LEVELLING UNDERLAYMENT COMPOUND

-	Type: Latex

-	Selection: As recommended by covering manufacturer.

M50/470	EXISTING FLOOR COVERINGS REMOVED

-	Substrate: Clear of covering and as much adhesive as possible. Skim with smoothing underlayment compound to give smooth, even surface.

LAYING COVERINGS

M50/640	ADHESIVE FIXING GENERALLY

-	Adhesive: Type to be as specified, recommended by covering/ underlay manufacturer or as approved.

-	Primer: Use and type as recommended by adhesive manufacturer.

-	Application: As necessary to achieve good bond.

-	Finished surface irregularities: Trowel ridges and high spots caused by particles on the substrate not acceptable.

M50/720	DOORWAYS

-	Joint location: On centre line of door leaf.

M50/740	EDGINGS/ COVER STRIPS

-	Manufacturer: Contractor’s choice

-	Product reference: Contractor’s choice subject to approval

-	Material/ finish: aluminium

-	Fixing: Secure (using matching fasteners where exposed to view) with edge of covering gripped.

M50/780	TRAFFICKING AFTER LAYING

-	Covering types: Linoleum

-	Traffic free period: To manufacturer’s recommendations

COMPLETION

M50/820	FINISHING LINOLEUM FLOORING

-	Cleaning operations:

-	Wash floor with water containing neutral (pH 6-9) detergent. If necessary, lightly scrub heavily soiled areas.

-	Rinse with clean water, removing surplus to prevent damage to adhesive. Allow to dry.

-	Emulsion polish: Two coats of a type recommended by covering manufacturer.

M50/880	WASTE

-	Spare covering material: Retain suitable material for patching. On completion submit pieces for selection. Hand over selected pieces to Employer.