M20	PLASTERED/ RENDERED/ ROUGHCAST COATINGS

To be read with Preliminaries/ General conditions.

TYPES OF COATING/130

M20/130	CEMENT:LIME:SAND EXTERNAL RENDER TO EXISTING BRICKWORK WALLS AS SHOWN ON DRAWINGS, AND TO NEW STUDWORK WALLS AS SHOWN

-	Substrate: Exisitng brickwork or new studwork.

-	Preparation: Remove all existing plaster surface where existing walls are currently internal.  All areas to receive expanded metal mesh as elsewhere described.

-	Cement:lime:sand mortar:

-	Procurement: Contractors choice

-	Pigment: Not required .

-	Undercoats:

-	Mix (cement:lime:sand): 1:1:5-6 .

Cement type: White Portland .

-	Thickness (excluding dubbing out and keys): 8 -12mm

-	Final coat:

-	Mix (cement:lime:sand): 1:2:8 .

Cement type: Portland

Other requirements: None

-	Thickness: 6 – 8mm

-	Finish: Plain .

-	Accessories: Stainless steel render stop beads as clause 636 + movement joints

160	M20/135CEMENT:SAND (AIR ENTRAINED) SUBSTRATES TO INTERNAL WALLS

-	Substrate: All new blockwork or brickwork, plus existing unplastered brickwork throughout area G13.

-	Preparation: Ensure sufficient key exists.

-		    Mortar: Contractors choice

-	Procurement: Contractors choice .

-		Coats: 1 or 2 as required

-	Mix: 1:1: 3-4 .

Cement type:Portland

-	Thickness (excluding dubbing out and keys): 8 -10mm .

-	Finish: Lightly scratched to receive finishing coat plaster.     .

-	Accessories: Render beads and stops

M20/200	GYPSUM PLASTER ON CEMENT GAUGED UNDERCOATS – FINSHING COAT TO RENDERED BACKGROUNDS

-	Substrate: Cement render

-	Preparation: See Clause 160

-	Final coat: Gypsum plaster to BS 1191-1, class B.

-	Manufacturer: Contractors choice

-	Thickness: 2-3mm

-	Finish: Steel smooth trowelled to receive paint finish as elsewhere described .

-	Accessories: Plaster skim beads and the like

M20/280	GYPSUM PLASTER SKIM COAT ON PLASTERBOARD

-	Plasterboard: Various types and thicknesses

-	Preparation: Bonding coat as recommended by Manufacturer

-	Plaster: Board finish/ finish plaster to BS 1191-1, class B.

-	Manufacturer: British Gypsum or equal

Product reference: Thistle board finishing plaster

-	Thickness: 2 - 3mm_ .

-	Finish: Smooth.

-	Accessories: Plaster skim beads and the like.

MATERIALS AND MAKING OF MORTAR

M20/430	READY-TO-USE CEMENT GAUGED MORTARS

-	Time and temperature limitations: Use within limits prescribed by mortar manufacturer.

-	Retempering: Restore workability with water only within prescribed time limits.

M20/438	CEMENTS FOR MORTARS

-	Cement: To BS EN 197-1 and CE marked.

-	Types:	Portland cement, CEM I.

Portland slag cement, CEM II/S.

Portland fly ash cement, CEM II/V or W.

-	Strength class: 32.5, 42.5 or 52.5.

-	White cement: To BS EN 197-1 and CE marked.

-	Type: Portland cement, CEM I.

-	Strength class: 52.5.

-	Sulfate resisting Portland cement: To BS 4027 and Kitemarked.

-	Strength class: 42.5.

-	Masonry cement: To BS EN 998-1 and Kitemarked.

-	Class: MC 12.5 (with air entraining agent).

M20/440	SAND FOR CEMENT GAUGED MORTARS

-	Standard: To BS EN 13139.

-	Grading: 0/2 or 0/4 (CP or MP); category 2 fines.

-	Colour and texture: Consistent. Obtain from one source.

M20/443	LIME FOR CEMENT GAUGED MORTARS

-	Standard: To BS EN 459-1.

-	Type: CL 90S.

M20/449	ADMIXTURES FOR CEMENT GAUGED MORTARS

-	Suitable admixtures: Select from:

-	Air entraining (plasticizing) admixtures: To BS EN 934-2 and compatible with other mortar constituents.

-	Other admixtures: Submit proposals.

-	Prohibited admixtures: Calcium chloride and any admixture containing calcium chloride.

M20/478	HYDRAULIC LIME

-	Standard: To BS EN 459-1.

-	Type: Natural hydraulic lime (NHL).

M20/481	READY PREPARED LIME PUTTY

-	Type: Slaked directly from CL 90 quicklime to BS EN 459-1, using an excess of water.

-	Maturation: In pits/ containers that allow excess water to drain away.

-	Density of matured lime putty: 1.3-1.4 kg/litre.

-	Maturation period before use (minimum): 90 days.

-	Storage: Prevent drying out or wetting. Protect from frost.

M20/495	MIXING

-	Render mortars (site-made):

-	Batching: By volume. Use clean and accurate gauge boxes or buckets.

-	Mix proportions: Based on damp sand. Adjust for dry sand.

-	Lime:sand: Mix thoroughly. Allow to stand, without drying out, for at least 16 hours before using.

-	Mixes: Of uniform consistence and free from lumps. Do not retemper or reconstitute mixes.

-	Contamination: Prevent intermixing with other materials.

M20/497	COLD WEATHER

-	General: Do not use frozen materials or apply coatings on frozen or frost bound substrates.

-	External work: Avoid when air temperature is at or below 5°C and falling or below 3°C and rising. Maintain temperature of work above freezing until coatings have fully hardened.

-	Internal work: Take precautions to enable internal coating work to proceed without detriment when air temperature is below 3°C.

PREPARING SUBSTRATES

M20/510	SUITABILITY OF SUBSTRATES

-	Soundness: Free from loose areas and significant cracks and gaps.

-	Cutting, chasing, making good, fixing of conduits and services outlets and the like: Completed.

-	Tolerances: Permitting specified flatness/ regularity of finished coatings.

-	Cleanliness: Free from dirt, dust, efflorescence and mould, and other contaminants incompatible with coatings.

M20/541	BONDING AGENT APPLICATION

-	General: Apply evenly to substrate to achieve effective bond of plaster/ render coat. Protect adjacent surfaces.

M20/566	REMOVING DEFECTIVE EXISTING PLASTER

-	Plaster for removal: Detached, soft, friable, badly cracked, affected by efflorescence or otherwise damaged.

-	Hollow, detached areas: Removing defective plaster. Cut back to a square, sound edge.

-	Faults in substrate (structural deficiencies, damp, etc.): Submit proposals.

-	Cracks:

-	Fine hairline cracking/ crazing: Leave.

-	Other cracks: : Fill with cement sand 1:5-6, leave down 2-3mm to receive.from adjacent areas to receive finishing plaster as clause 200 .

-	Dust and loose material: Remove from exposed substrates and edges.

M20/568	EXISTING DAMP AFFECTED PLASTER/ RENDER

-	Plaster affected by rising damp: Remove to a height of 300 mm above highest point reached by damp or 1 m above dpc, whichever is higher.

-	Perished and salt contaminated masonry:

-	Mortar joints: Rake out.

-	Masonry units: Submit proposals.

-	Faults in substrate (structural deficiencies, additional sources of damp, etc.): Submit proposals.

-	Drying out substrates: Established drying conditions. Leave walls to dry for as long as possible before plastering.

-	Dust and loose material: Remove from exposed substrates and edges.

BACKINGS/ BEADS/ JOINTS

M20/605	GYPSUM PLASTERBOARD BACKINGS

-	Type: To BS 1230, type 1.

-	Core density (minimum): 650 kg/m3.

-	Exposed surface and edge profiles: Suitable to receive specified plaster finish.

M20/607	PROPRIETARY GYPSUM PLASTERBOARD BACKINGS WITH METAL FURRINGS

-	Manufacturer: British Gypsum

-	Product reference: Gypliner furrings

-	Exposed surface and edge profiles: Suitable to receive specified plaster finish.

M20/612	JOINTS IN PLASTERBOARD BACKINGS

-	Ceilings:

-	Bound edges: At right angles to supports and with ends staggered in adjacent rows.

-	Two layer boarding: Stagger joints between layers.

-	Partitions/ walls:

-	Vertical joints: Centre on studs. Stagger joints on opposite sides of studs.

Two layer boarding: Stagger joints between layers.

-	Horizontal joints:

Two layer boarding: Stagger joints between layers by at least 600 mm. Support edges of outer layer.

-	Joint widths (maximum): 3 mm.

M20/630	BEADS/ STOPS FOR INTERNAL USE

-	Material: Galvanized steel to BS 6452-1.

M20/636	BEADS/ STOPS FOR EXTERNAL USE

- Stainless steel: To BS EN 10088-1, grade 1.4301.

M20/640	BEADS/ STOPS GENERALLY

-	Location: External angles and stop ends, except where specified otherwise.

-	Corners: Neat mitres at return angles.

-	Fixing: Secure, using longest possible lengths, plumb, square and true to line and level, ensuring full contact of wings with substrate.

-	Beads/ stops for external render: Fix mechanically.

-	Finishing: After coatings have been applied remove surplus material, while still wet, from surfaces of beads/ stops exposed to view.

M20/646	CRACK CONTROL AT JUNCTIONS BETWEEN DISSIMILAR SOLID SUBSTRATES

-	Locations: Where defined movement joints are not required. Where dissimilar solid substrate materials are in same plane and rigidly bonded or tied together.

-	Crack control materials:

-	Isolating layer: Building paper to BS 1521.

-	Metal lathing: ______ .

-	Installation: Fix metal lathing over isolating layer. Stagger fixings along both edges of lathing.

-	Width of installation over single junctions:

-	Isolating layer: 150 mm.

-	Lathing: 300 mm.

-	Width of installation across face of dissimilar substrate material (column, beam, etc. with face width not greater than 450 mm):

-	Isolating layer: 25 mm (minimum) beyond junctions with adjacent substrate.

-	Lathing: 100 mm (minimum) beyond edges of isolating layer.

M20/659	PLASTERBOARD JOINTS

-	Joints and angles (except where coincident with metal beads): Reinforce with continuous lengths of jointing tape.

MOULDINGS/ DECORATIVE PLASTERWORK

INTERNAL PLASTERING

M20/710	APPLICATION GENERALLY

-	Application of coatings: Firmly and in one continuous operation between angles and joints. Achieve good adhesion.

-	Appearance of finished surfaces: Even and consistent. Free from rippling, hollows, ridges, cracks and crazing.

-	Accuracy: Finish to a true plane, to correct line and level, with angles and corners to a right angle unless specified otherwise, and with walls and reveals plumb and square.

-	Drying out: Prevent excessively rapid or localised drying out.

M20/715	FLATNESS/ SURFACE REGULARITY

-	Sudden irregularities: Not permitted.

-	Deviation of plaster surface: Measure from underside of a straight edge placed anywhere on surface.

-	Permissible deviation (maximum) for plaster not less than 13 mm thick: 3 mm in any consecutive length of 1800 mm.

M20/720	DUBBING OUT

-	General: Correct substrate inaccuracies.

-	New smooth, dense concrete and similar surfaces: Dubbing out prohibited unless total plaster thickness is within range recommended by plaster manufacturer.

-	Thickness of any one coat (maximum): 10 mm.

-	Mix: As undercoat.

-	Application: Achieve firm bond. Allow each coat to set sufficiently before the next is applied. Cross scratch surface of each coat.

M20/725	UNDERCOATS GENERALLY

-	General: Rule to an even surface. Cross scratch to provide a key for the next coat.

-	Undercoats on metal lathing: Work well into interstices to obtain maximum key.

-	Undercoats gauged with Portland cement: Do not apply next coat until drying shrinkage is substantially complete.

M20/777	SMOOTH FINISH

-	Appearance: A tight, matt, smooth surface with no hollows, abrupt changes of level or trowel marks. Avoid water brush, excessive trowelling and over polishing.

M20/778	WOOD FLOAT FINISH

-	Appearance: An even overall texture. Finish with a dry wood float as soon as wet sheen has disappeared.

EXTERNAL RENDERING

M20/810	APPLICATION GENERALLY

-	Application of coatings: Firmly and in one continuous operation between angles and joints. Achieve good adhesion.

-	Appearance of finished surfaces: Even and consistent. Free from rippling, hollows, ridges, cracks and crazing.

-	Accuracy: Finish to a true plane, to correct line and level, with angles and corners to a right angle unless specified otherwise, and with walls and reveals plumb and square.

-	Drying: Prevent excessively rapid or localized drying out.

M20/815	FLATNESS/ SURFACE REGULARITY OF RENDERING TO RECEIVE CERAMIC TILES

-	Sudden irregularities: Not permitted.

-	Deviation of render surface: Measure from underside of a 2 m straight edge placed anywhere on surface.

-	Permissible deviation (maximum): 3 mm.

M20/820	DUBBING OUT FOR RENDERING

-	General: Correct substrate inaccuracies.

-	Thickness of any one coat (maximum): 16 mm.

-	Total thickness (maximum): 20 mm, otherwise obtain instructions.

-	Mix: As undercoat.

-	Application: Achieve firm bond. Allow each coat to set sufficiently before the next is applied. Comb surface of each coat.

M20/840	UNDERCOATS GENERALLY

-	General: Rule to an even surface. Comb to provide a key for the next coat. Do not penetrate the coat.

-	Undercoats on metal lathing: Work well into interstices to obtain maximum key.

M20/856	FINAL COAT - PLAIN FLOATED FINISH

-	Finish: Even, open texture free from laitance.

M20/880	CURING AND DRYING

-	General: Prevent premature setting and uneven drying of each coat.

-	Curing coatings: Keep each coat damp by covering with polyethylene sheet and/ or spraying with water.

-	Curing period (minimum): ______ .

-	Final coat: Hang sheeting clear of the final coat.

-	Drying: Allow each coat to dry thoroughly, with drying shrinkage substantially complete before applying next coat.

-	Protection: Protect from frost and rain.

M20/885	CURING AND DRYING NONHYDRAULIC LIME RENDER

-	General: Prevent premature setting and uneven drying of each coat.

-	Curing coatings: Keep each coat damp by covering with sheeting hung clear of coating. Spray with water until sufficiently firm.

-	Sheeting: ______ .

-	Shrinkage: Thoroughly consolidate/ scour each coat one or more times as necessary to control shrinkage.