Z11	PURPOSE MADE METALWORK

To be read with Preliminaries/ General conditions.

PRODUCTS

Z11/310	MATERIALS GENERALLY

•	 Grades of metals, section dimensions and properties: To appropriate British Standards.

When not specified, select grades and sections appropriate for the purpose.

•	 Prefinished metal: May be used if methods of fabrication do not damage or alter

appearance of finish, and finish is adequately protected.

•	 Fasteners: To appropriate British Standards and, unless specified otherwise, of same

metal as component being fastened, with matching coating or finish.

FABRICATION

Z11/510	PREPARATION FOR APPLICATION OF COATINGS

-	General: Complete fabrication, and drill fixing holes before applying coatings.

-	Paint, grease, flux, rust, burrs and sharp arrises: Remove.

Z11/515	FABRICATION GENERALLY

-	Contact between dissimilar metals in components: Avoid.

-	Finished components: Rigid and free from distortion, cracks, burrs and sharp arrises.

-	Moving parts: Free moving without binding.

-	Corner junctions of identical sections: Mitre.

-	Prefinished metals: Do not damage or alter appearance of finish.

Z11/520	COLD FORMED WORK

-	Profiles: Accurate, with straight arrises.

Z11/527	WELDINGRAILINGS, BALUSTRADES, HANDRAILS, CANOPY ROOF STRUCTURES.

•	 Welding procedures:

-	Method and standard: Metal arc welding to BS EN 1011-1 and -2..

-	Welding Procedure Specification (WPS): See engineers requirements.

•	 Preparation:

-	Joint preparation: Clean thoroughly.

-	Surfaces of materials that will be self-finished and visible in the completed work:

protect from weld splatter.

•	 Jointing:

- Joints: Fully bond parent and filler metal throughout with no inclusions, holes,

porosity or cracks.

-	Dissimilar metals: Not applicable.

-	Strength requirements: Welds to achieve design loads.

-	Heat straightening: Submit proposals.

-	Complex assemblies: Agree priority for welding members to minimize distortion

caused by subsequent welds.

-	Tack welds: Use only for temporary attachment.

-	Jigs: Provide to support and restrain members during welding.

-	Filler plates: Submit proposals.

-	Lap joints: Minimum 5 x metal thickness or 25 mm, whichever is greater.

-	Weld terminations: Clean and sound.

Z11/710	FINISHING WELDED AND BRAZED JOINTS VISIBLE IN COMPLETE WORK

-	Butt joints: Smooth, and flush with adjacent surfaces.

-	Fillet joints: Neat.

-	Grinding: Grind smooth where indicated on drawings.

745	PREPARATION FOR APPLICATION OF COATINGS

•	 General: Complete fabrication, and drill fixing holes before applying coatings.

•	 Paint, grease, flux, rust, burrs and sharp arrises: Remove.

780	GALVANIZING

•	 Standard: To BS EN ISO 1461.

•	 Preparation:

-	Vent and drain holes: Provide in accordance with BS EN 14713. Seal after sections have been drained and cooled.

-	Components subjected to cold working stresses: Heat treat to relieve stresses

before galvanizing.

-	Welding slag: Remove.

-	Component cleaning: To BS EN ISO 8501-1.

Grade: St 2½