M40	STONE/ CONCRETE/ QUARRY/ CERAMIC TILING/ MOSAIC

To be read with Preliminaries/ General conditions.

TYPES OF TILING/ MOSAIC

M40/110	TILING TO WALLS IN WC’S, STORAGE/WET AREAS, CLEANERS’ STORES, KITCHEN AREA G06, TEA POINT AREA G07, AS SHOWN ON DRAWINGS

-	Tiles:

-	Manufacturer/ Supplier:Contractor’s choice .

-	Colour: to be selected .

-	Finish: glazed .

-	Size: 97 x 97 .

-	Background/ Base: existing plaster and new plaster skim .

-	Bedding: Thin bed adhesive – ribbed as clasue 650 .

-	Reinforcement: None .

-	Adhesive: Ardex Ardipox WA or equal approved .

-	Joint width: 3mm .

-	Grout:Ardurit FS white .

-	Movement joints: As clause 815 at internal corners of rooms .

M40/110A	QUARRY TILING TO FLOORS WHERE SHOWN ON DRAWINGS

-	Tiles: quarry tiles .

-	Manufacturer/ Supplier: Dennis Ruabon .

Product reference: Quarrundum .

-	Colour: TBC .

-	Size: 194 x 194 .

-	Thickness: 12.5 .

-	Slip potential: slip resistant

-	Background/ Base: screed .

-	Preparation: thoroughly cleaned .

-	Intermediate substrate: not required

-	Bedding: solid bed as clause 710, 3-5mm thick .

-	Reinforcement: not required .

-	Adhesive: Ardex S21 cement based .

-	Joint width: 6mm .

-	Grout: Ardex epoxy grout .

-	Movement joints: As recommended by manufacturer .

-	Accessories: Matching 150 high round topped coved skirtings with all internal and external angles etc.

GENERAL

M40/210	SUITABILITY OF BACKGROUNDS/ BASES

-	Background/ base tolerances: To permit specified flatness/ regularity of finished surfaces given the permissible minimum and maximum thickness of bedding.

-	New background drying times (minimum):

-	Concrete walls: 6 weeks.

-	Brick/ block walls: 6 weeks.

-	Rendering: 2 weeks.

-	Gypsum plaster: 4 weeks.

-	New base drying times (minimum):

-	Concrete slabs: 6 weeks.

-	Cement:sand screeds: 3 weeks.

M40/215	FALLS IN THE BASES

-	General: Give notice if falls are inadequate.

M40/250	SAMPLES

-	General: Submit representative samples of the following: all tiles .

PREPARATION

M40/310	EXISTING BACKGROUNDS/ BASES GENERALLY

-	Efflorescence, laitance, dirt and other loose material: Remove.

-	Deposits of oil, grease and other materials incompatible with the bedding: Remove.

-	Tile, paint and other nonporous surfaces: Clean.

-	Wet backgrounds: Dry before tiling.

M40/320	EXISTING CONCRETE/ SCREEDS

-	Loose or hollow portions: Cut out.

-	Making good: material recommended by tiling adhesive manufacturer .

M40/330	EXISTING PLASTER

-	Defective areas: Remove plaster that is loose, soft, friable, badly cracked or affected by efflorescence. Cut back to straight horizontal and vertical edges.

-	Making good: Use plaster or nonshrinking filler.

M40/340	EXISTING GLAZED BRICK

-	Defective areas: Cut out.

-	Making good: Material recommended by adhesive manufacturer .

M40/360	EXISTING PAINT

-	Paint with unsatisfactory adhesion: Remove so as not to impair bedding adhesion.

M40/370	NEW IN SITU CONCRETE

-	Backgrounds/ bases to be tiled: Remove mould oil, surface retarders and other materials incompatible with bedding.

M40/380	NEW PLASTER

-	Plaster: Dry, solidly bedded, free from dust and friable matter.

-	Plaster primer: Apply if recommended by adhesive manufacturer.

M40/390	PLASTERBOARD BACKGROUNDS

-	Boards: Dry, securely fixed and rigid with no protruding fixings and face to receive decorative finish exposed.

M40/450	PREPARING CONCRETE BASES FOR UNBONDED BEDDING - WITHOUT SEPARATING LAYER

-	Surface finish: Smooth.

-	Surface preparation: Dampen lightly before laying mortar bed.

M40/460	SMOOTHING UNDERLAYMENT

-	Type: Recommended by adhesive manufacturer.

-	Condition: Allow to dry before tiling.

FIXING

M40/510	FIXING GENERALLY

-	Colour/ shade: Unintended variations within tiles for use in each area/ room are not permitted.

-	Variegated tiles: Mix thoroughly.

-	Adhesive: Compatible with background/ base. Prime if recommended by adhesive manufacturer.

-	Cut tiles: Neat and accurate.

-	Fixing: Provide adhesion over entire background/ base and tile backs.

-	Final appearance: Before bedding material sets, make adjustments necessary to give true, regular appearance to tiles and joints when viewed under final lighting conditions.

-	Surplus bedding material: Clean from joints and face of tiles without disturbing tiles.

M40/530	SETTING OUT

-	Joints: True to line, continuous and without steps.

-	Joints on walls: Horizontal, vertical and aligned round corners.

-	Joints in floors: Parallel to the main axis of the space or specified features.

-	Cut tiles: Minimize number, maximize size and locate unobtrusively.

-	Joints in adjoining floors and walls: Align.

-	Joints in adjoining floors and skirtings: Align.

-	Movement joints: Where locations are not indicated, submit proposals.

M40/550	FLATNESS/ REGULARITY OF TILING

-	Sudden irregularities: Not permitted.

-	Deviation of surface: Measure from underside of a 2 m straightedge placed anywhere on surface. The straightedge should not be obstructed by the tiles and no gap should be greater than 3 mm.

M40/560	LEVEL OF TILING ACROSS JOINTS

-	Deviation (maximum) between tile surfaces either side of any type of joint:

-	1 mm for joints less than 6 mm wide.

-	2 mm for joints 6 mm or greater in width.

M40/570	MORTAR BEDDING

-	Bedding mix:

-	Cement: Portland to BS EN 197-1 type CEM I/42.5.

-	Sand for walls: To BS 1199, type A.

-	Sand for floors: To BS EN 13139.

-	Grading designation: 0/4 (MP) category 1 fines and between 20%-66% passing a 0.5 sieve.

-	Batching: Select from:

-	Batch by weight.

-	Batch by volume: Permitted on the basis of previously established weight:volume relationships of the particular materials. Use accurate gauge boxes. Allow for bulking of damp sand.

-	Mixing: Mix materials thoroughly to uniform consistence. Use a suitable forced action mechanical mixer. Do not use a free fall type mixer.

-	Application: At normal temperatures use within two hours. Do not use after initial set. Do not retemper.

M40/590	COVED TILE SKIRTINGS

-	Sequence: Bed solid to wall before laying floor tiles.

-	Bedding: Cement based adhesive. .

M40/650	THIN BED ADHESIVE - RIBBED (WALLS)

-	Application: Apply 3 mm floated coat of adhesive to dry background in areas of approximately 1 m2. Trowel to ribbed profile.

-	Tiling: Press tiles firmly onto float coat.

M40/710	THICK BED ADHESIVE - SOLID (FLOORS)

-	Application: Apply floated coat of adhesive to dry base and comb surface.

-	Tiling: Apply coat of adhesive to backs of tiles, filling depressions or keys. Press tiles firmly into position.

-	Finished adhesive thickness: Within range recommended by manufacturer.

MOVEMENT JOINTS/ GROUTING/ COMPLETION

M40/815	SEALANT MOVEMENT JOINTS WHERE REQUIRED

-	Joints: Extend through tiles and bedding to base/ background. Centre over joints in base/ background.

-	Width: To be agreed _.

-	Sealant: To be agreed .

-	Preparation and application: As section Z22.

M40/875	GROUTING

-	Sequence: Grout when bed/ adhesive has set sufficiently to prevent disturbance of tiles.

-	Joints: 6 mm deep (or depth of tile if less). Free from dust and debris.

-	Grouting: Fill joints completely, tool to profile, clean off surface. Leave free from blemishes.

-	Polishing: When grout is hard, polish tiling with a dry cloth.