Z33	ANODIZING

To be read with Preliminaries/ General conditions

Z33/110	ANODIC COATING

-	Selected anodizer: Submit details before commencement of anodizing.

Z33/210	WORKING PROCEDURES

-	Requirement: Comply with BS 3987 for anodic coatings on wrought aluminium.

Z33/220	ANODIZER REQUIREMENTS

-	Processing:

-	Approved by the Aluminium Finishing Association.

-	Currently certified to BS EN ISO 9001.

-	Each anodizer to use only one plant.

Z33/230	GUARANTEES

-	Anodizer guarantees:

-	Submit sample copies before commencement of anodizing.

-	Submit signed project specific copies on completion of work.

Z33/310	PRETREATMENT

-	Condition of components to be anodized:

-	Free from corrosion and damage.

-	Suitable for and compatible with the pretreatment and anodizing process.

-	Process: In accordance with the specification requirements for the finish.

Z33/410	EXTENT OF ANODIC COATINGS

-	Application: To visible component surfaces, and concealed surfaces requiring protection. Coated surfaces will be deemed ‘significant surfaces’ for relevant BS 3987 performance requirements.

Z33/420	APPLICATION OF ANODIC COATINGS

-	Surfaces to receive anodic coatings: Clean.

-	Jig points: To be agreed. Not on visible areas of anodic coated components.

-	Use of touch-up paint: Not acceptable.

Z33/430	PERFORMANCE AND APPEARANCE OF ANODIC COATINGS

-	Standard: To BS 3987.

-	Visual inspection after anodizing: Significant surfaces to be free from visible coating/ defects when viewed from a distance of not less than 5 m for external and 3 m for internal applications.

Z33/440	FABRICATIONS

-	 Units may be assembled:

-	Before anodizing, subject to satisfactory drainage.

-	From components anodized after cutting to size.

-	Where approved, from components anodized before cutting to size.

Z33/450	FABRICATION DAMAGE REPAIR/ REPLACEMENT

-	Inspection: Check all components before delivery to site for damage to anodic coatings. Submit proposals for repair or replacement.

Z33/510	PROTECTION

-	Anodic coated surfaces of components: Protect from damage during handling and installation, or by subsequent site operations.

-	Protective coverings: Must be:

-	Resistant to weather conditions.

-	Partially removable to suit building in and access to fixing points.

-	Protective tapes in contact with anodizing: Must be:

-	Low tack, self adhesive and light in colour.

-	Applied and removed in accordance with tape and anodizers recommendations.

-	Inspection of protection: Carry out monthly. Promptly repair any deterioration or deficiency.

Z33/520	SITE DAMAGE REPAIR/ REPLACEMENT

-	Damage to anodic coatings: Rectify immediately damage caused during handling and installation, or by subsequent site operations. Submit proposals for extensive repair or replacement.

Z33/540	COMPLETION

-	Cleaning and maintenance of anodic coated surfaces: Carry out in accordance with procedures detailed in the anodizer’s guarantees.