H72	ALUMINIUM STRIP/ SHEET COVERINGS/ FLASHINGS

To be read with Preliminaries/ General conditions.

TYPES OF ALUMINIUM WORK

H72/250	WEATHERING TO BRICK PLINTH BELOW TIMBER WEATHERBOARDING

-	Substrate: chamfered timber grounds.

-	Underlay: not required.

-	Aluminium: as clause 525.

-	Alloy designation: EN AW-1050A.

-	Temper: 0.

-	Finish: Polyester powder coating.

-	Thickness: 3.0mm.

-	Joints: proprietary jointing straps with neoprene seal.

-	Spacing: as few as possible.

-	Edge details: beaded drip at front, upstand at rear.

-	Fixing: fixed clips at max. 400mm cc.

- Other requirements: preformed stop ends at door opening G06D1; preformed corner sections; preformed upstand sections at junctions with existing building.

H72/252	POWDER COATED COPINGS TO RENDERED PARAPETS	-	Substrate: Studwork with ply backing .

-		-Manufacturer: Dales Fabrications Ltd. Crompton Road Industrial Estate Ilkeston, Derby DE7 4BG

Product Reference : Meridian Coping System, profile see detail drawings

-	Material grade designation: Aluminium sheet to EN 485/515/573: Designation NS3, condition H14.

- 	Thickness: 2.0mm.

-	Finish: Polyester powder coating.

-	Joints: Brackets fixed with No 12 x50mm stainless steel screws and rawlplugs into blockwork generally at 1500 c/c’s.

-	Fixing: As manufacturers recommendation

Accessories: Polyester coated joint straps,stop ends, internal and external cornersFixings and joint sealant as recommended for the purpose and supplied by Dales  Fabrications Ltd.

GENERAL REQUIREMENTS/ PREPARATORY WORK

H72/510	WORKMANSHIP GENERALLY

-	Standard: Generally to CP 143-15.

-	Fabrication and fixing: To provide a secure, free draining and completely weathertight installation.

-	Operatives: Trained in the application of aluminium coverings/ flashings. Submit records of experience on request.

-	Measuring, marking, cutting and forming: Prior to assembly wherever possible.

-	Marking out: With pencil, chalk or crayon. Do not use scribers or other sharp instruments without approval.

-	Folding: With mechanical or manual presses to give straight, regular and tight bends, leaving panels free from ripples, kinks, buckling and cracks. Use hand tools only for folding details that cannot be pressed.

-	Surface protection: Fully coat surfaces to be embedded in concrete or mortar with high build bitumen based paint, after folding.

-	Sharp metal edges: Fold under or remove as work proceeds.

-	Joints: Do not use sealants to attain waterproofing.

-	Finished aluminium work: Fully supported, adequately fixed to resist wind uplift and able to accommodate thermal movement without distortion or stress.

-	Protection: Prevent staining, discolouration and damage by subsequent works.

H72/515	WELDING

- In situ welding: Not permitted.

H72/520	ALUMINIUM STRIP/ SHEET

-	Standard: To BS EN 485, BS EN 507, BS EN 515 and BS EN 573.

-	Stamped or labelled with alloy designation, temper, finish and thickness.

-	Manufacturer: Contractor’s choice.

H72/525	COATED ALUMINIUM  STRIP/ SHEET

- Manufacturer: Contractor’s choice – polyester powder coated to match window cladding.

H72/526	COATED ALUMINIUM  STRIP/ SHEET

-	Manufacturer: Contractor’s choice – preweathered zinc coated.

H72/610	SUITABILITY OF SUBSTRATES

-	Condition: Dry and free of dust, debris, grease and other deleterious matter.

H72/620	PREPARATION OF EXISTING TIMBER SUBSTRATES

-	Remedial work: Adjust boards to level and securely fix. Punch in any protruding fasteners and plane or sand to achieve an even surface.

-	Defective boards: Give notice.

-	Moisture content: Not more than 22% at time of covering.

H72/640	TIMBER FOR USE WITH ALUMINIUM WORK

-	Quality: Planed, free from wane, splits, pitch pockets, decay and insect attack (ambrosia beetle excepted).

-	Moisture content: Not more than 22% at time of covering.

-	Preservative treatment: Organic solvent as section Z12, and British Wood Preserving and Damp-proofing Association Manual - Commodity Specification C8.

H72/650	UNDERLAY

-	Handling: Prevent tears and punctures.

-	Laying: Butt jointed onto a dry substrate.

-	Fixing edges: With aluminium or galvanized steel staples or clout nails.

-	Do not lay over eaves and drip/ step aluminium underlaps.

-	Protection: Keep dry and cover with aluminium at the earliest opportunity.

FIXING

H72/710	FIXINGS FOR CLIPS

-	Nails to timber substrates: Aluminium to BS 1202-3 for aluminium clips. Stainless steel (austenitic) for stainless steel clips.

-	Shank type: Annular ringed or helical threaded.

-	Shank diameter: Not less than 2.65 mm.

-	Head: Flat.

-	Length: Not less than 25 mm or equal to substrate thickness.

-	Screws to concrete/ masonry substrates:  Sherardized or zinc plated steel to BS 1210, table 2, or aluminium to BS 1210, table 5 for aluminium clips. Stainless steel (austenitic) to

BS 1210, table 4 for stainless steel clips.

-	Diameter: Not less than 3.35 mm.

-	Length: Not less than 25 mm.

-	Washers and plastic plugs: Compatible with screws.

-	Screws to composite metal decks: Self tapping, as recommended by the deck and aluminium manufacturer/ supplier for aluminium or stainless steel clips.

H72/750	CLIPS FOR FLASHINGS/ CROSS JOINTS

-	Material: Cut from same alloy and thickness as that being secured.

-	Dimensions:

-	Width: Not less than 50 mm.

-	Length: Sufficient to suit detail.

-	Fixing: Secure each clip to substrate with two fixings, not more than 50 mm from edge of strip/ sheet being fixed.

H72/790	SCREW FIXING

-	Fixing: use sherardized, zinc plated steel or aluminium screws and washers at not more than 400 mm centres, at every change of direction, and with at least two fixings for each piece of aluminium.

JOINTING

H72/815	FREE EDGE DETAILS

-	Visible feature edges: Finish with 13mm beads centred on plane of panels