M60	PAINTING/ CLEAR FINISHING

To be read with Preliminaries/ General conditions.

Note that this section applies to the following areas:

All new external render,  joinery and metalwork

External surfaces of all windows on north elevation

All internal surfaces except those on 1st and 2nd floors to the south of DF27A/B and DS24A/B

COATING SYSTEMS

M60/110	DULUX TRADE DIAMOND MATT PAINT TO INTERNAL PLASTERED SURFACES, CONCRETE CEILINGS, AND PREVIOUSLY PAINTED BRICKWORK

-	Manufacturer: as clause 210.

-	Surfaces:.

- Preparation:

- Existing: refer to clauses 400, 440 & 622

- New : refer to clauses 570, 580.

-	Initial coats: 1 Nº mist coat.

-	Finishing coats: Sufficient coats to give solid colour

M60/130	GLOSS PAINT

-	Manufacturer: as clause 210.

-	Surfaces: New external joinery

- Preparation: Patch prime only to existing surfaces.

- Existing: refer to clauses 400, 440, 461 , 490, 622, 631, .

-	Initial coats: 2 coats undercoat.

-	Finishing coats: Sufficient coats to give solid colour.

130A	GLOSS PAINT TO EXTERNAL METALWORK

•	 Manufacturer: Dulux or similar approved.

Surfaces: galvanised.

-	Preparation: scrub with Dulux Oil and Grease Remover, rinse and allow to dry.

•	 Initial coats: Dulux Trade Metalshield Quick drying Metal Primer.

-	Number of coats: 1.

•	 Finishing coats: Dulux Trade Metalshield Gloss Finish.

-	Number of coats: 2.

M60/150	DULUX TRADE DIAMOND QUICK DRYING EGGSHELL PAINT

-	Manufacturer: as clause 210.

-	Surfaces: Internal exposed pipework, timber and mdf, except where indicated in clause 161.

- Preparation: Patch prime only to existing surfaces.

- Existing: refer to clauses 400, 440, 461 , 490, 622, 631, .

- New : refer to clauses 471 & 481, 500, 511, 521

-	Initial coats: 1 coat primer, 2 coats undercoat.

-	Finishing coats: Sufficient coats to give solid colour.

M60/160	EXTERIOR DECORATIVE WOODSTAIN.

-	Manufacturer: Sadolins or as clause 210.

-	Surfaces: New external plywood & benches.

-	Initial coats: 1 coat Weathershield Exterior Woodstain.

-	Finishing coats: 1 coat Weathershield Exterior Woodstain.

M60/161	VARNISH

-	Manufacturer: Sadolins.

-	Surfaces: New birch faced ply

-	Initial coats and finishing coats: clear satin varnish, sanded between coats, and sufficient to give a smooth even finish

M60/170	MASONRY COATING TO EXTERNAL RENDERED SURFACES

-	Manufacturer: Keim Paints Ltd.

-	Product reference: Keim Granital.

-	Surfaces: External render.

-	Preparation: Leave new render for minimum 15 days to dry out.

-	Initial coats:

-	Type: As manufacturer’s recommendations.

-	Number of coats: As manufacturer’s recommendations.

-	Finishing coats:

-	Type: As manufacturer’s recommendations.

-	Number of coats: As manufacturer’s recommendations.

M60/180	FLOOR COATING

-	Manufacturer: Contractor’s choice .

-	Surfaces: Exisitng and new screed area G23 .

-	Preparation and coating: As manufacturer’s recommendations .

GENERALLY

M60/210	COATING MATERIALS

- Manufacturer: Obtain coatings from Dulux or equal approved.

M60/215	HANDLING AND STORAGE

-	Coating materials: Deliver in sealed containers, labelled clearly with brand name, type of material and manufacturer’s batch number.

-	Materials from more than one batch: Store separately. Allocate to distinct parts or areas of the work.

M60/240	SURFACES NOT TO BE COATED

-	New galvanised external metalwork to playground canopy

M60/280	PROTECTION

- ‘Wet paint’ signs and barriers: Provide where necessary to protect other operatives and the general public, and to prevent damage to freshly applied coatings.

PREPARATION

M60/400	PREPARATION GENERALLY

-	Standard: To BS 6150, Section 4.

-	Preparation materials: Types recommended by their manufacturers and the coating manufacturer for the situation and surfaces being prepared.

-	Substrates: Sufficiently dry in depth to suit coating.

-	Efflorescence salts: Remove.

-	Dirt, grease and oil: Remove.

-	Give notice if contamination of surfaces/ substrates has occurred.

-	Joints, cracks, holes and other depressions:

-	Fill with stoppers/ fillers. Work well in and finish off flush with surface.

-	Abrade to a smooth finish.

-	Water based stoppers and fillers:

-	Apply before priming unless recommended otherwise by manufacturer.

-	If applied after priming: Patch prime.

-	Oil based stoppers and fillers: Apply after priming.

-	Surface irregularities: Abrade to a smooth finish.

-	Dust, particles and residues from abrasion: Remove.

-	Doors, opening windows and other moving parts:

-	Ease before coating.

-	Prime resulting bare areas.

M60/425	IRONMONGERY

-	Before commencing work: Remove ironmongery from surfaces to be coated.

-	Hinges: Do not remove.

-	On completion of coating work: Refix.

M60/430	EXISTING IRONMONGERY

-	General: Remove old coating marks. Clean and polish.

M60/440	PREVIOUSLY COATED SURFACES GENERALLY

-	Preparation standard: To BS 6150, Section 6.

-	Removing coatings: Do not damage substrate and adjacent surfaces or adversely affect subsequent coatings.

-	Loose, flaking or otherwise defective areas: Carefully remove to a firm edge.

-	Alkali affected coatings: Completely remove.

-	Discovery: Give notice of:

-	Coatings suspected of containing lead.

-	Substrates suspected of containing asbestos.

-	Significant rot, corrosion or other degradation of substrates.

-	Retained coatings:

-	Thoroughly clean to remove dirt, grease and contaminants.

-	Gloss coated surfaces: Abrade to provide a key.

-	Partly removed coatings:

-	Additional preparatory coats: Apply to restore original coating thicknesses.

-	Junctions: Abrade to give a flush surface.

-	Completely stripped surfaces: Prepare as for uncoated surfaces.

M60/461	PREVIOUSLY COATED TIMBER

-	Degraded or weathered surface timber: Abrade to remove.

-	Degraded substrate timber: Repair with sound timber of same species.

-	Exposed resinous areas and knots: Apply two coats of knotting.

M60/471	PREPRIMED TIMBER

-	Defective primer: Abrade back to bare timber.

-	Bare areas: Reprime.

M60/481	UNCOATED TIMBER

-	General: Abrade to a smooth, even finish with arrises and moulding edges lightly rounded or eased.

-	Heads of fasteners: Countersink sufficient to hold stoppers/ fillers.

-	Resinous areas and knots: Apply two coats of knotting.

M60/490	PREVIOUSLY COATED STEEL

-	Defective paintwork: Remove to leave a firm edge and clean bright metal.

-	Sound paintwork: Abrade to provide key for subsequent coats.

-	Corrosion and loose scale: Abrade back to bare metal.

-	Residual rust: Treat with a proprietary removal solution.

-	Bare metal: Apply primer as soon as possible.

-	Remaining areas: Degrease.

M60/500	PREPRIMED STEEL

-	Defective primer, corrosion and loose scale: Abrade back to bare metal.

-	Bare areas: Reprime as soon as possible.

M60/511	GALVANIZED, SHERARDIZED AND ELECTROPLATED STEEL

-	White rust: Remove.

-	Pretreatment: Apply one of the following:

-	‘T wash’/ mordant solution to blacken whole surface.

-	Etching primer recommended by coating system manufacturer.

M60/521	UNCOATED STEEL - MANUAL CLEANING

-	Oil and grease: Remove.

-	Corrosion, loose scale, welding slag and spatter: Abrade to remove.

-	Residual rust: Treat with a proprietary removal solution.

-	Primer: Apply as soon as possible.

M60/570	UNCOATED MASONRY/ RENDERING

-	Loose and flaking material: Remove.

M60/580	UNCOATED PLASTER

-	Nibs, trowel marks and plaster splashes: Scrape off.

-	Overtrowelled ‘polished’ areas: Abrade lightly.

M60/590	UNCOATED PLASTERBOARD

-	Depressions around fixings: Fill with stoppers/ fillers.

M60/622	ORGANIC GROWTHS

-	Loose growths and infected coatings: Scrape off and remove.

-	Treatment biocide: Apply appropriate solution to growth areas and surrounding surfaces.

-	Dead growth: Scrape off and remove.

-	Residual effect biocide: Apply appropriate solution to inhibit re-establishment of growths.

M60/631	PREVIOUSLY PAINTED WINDOW FRAMES

-	Paint encroaching beyond glass sight line: Remove.

-	Loose and defective putty: Remove.

-	Putty cavities and junctions between previously painted surfaces and glass: Clean thoroughly.

-	Finishing:

-	Patch prime, reputty and allow to set.

-	Seal and coat as soon as sufficiently hard.

M60/640	EXTERNAL POINTING TO EXISTING FRAMES

-	Defective sealant pointing: Remove.

-	Joint depth: Approximately half joint width; adjust with backing strip if necessary.

-	Preparation and application: As section Z22.

-	Sealant:

-	Manufacturer: Contractors choice.

M60/645	POINTING TO INTERNAL MOVEMENT JOINTS

-	General: Apply to junctions of walls and ceilings with architraves, skirtings and other trims.

-	Preparation and application: As section Z22.

-	Sealant: Water based acrylic.

-	Manufacturer: Contractors choice.

APPLICATION

M60/711	COATING GENERALLY

-	Application standard: To BS 6150, Section 5.

-	Conditions: Maintain suitable temperature, humidity and air quality during application and drying.

-	Surfaces: Clean and dry at time of application.

-	Thinning and intermixing of coatings: Not permitted unless recommended by manufacturer.

-	Overpainting: Do not paint over intumescent strips or silicone mastics.

-	Priming coats:

-	Thickness: To suit surface porosity.

-	Application: As soon as possible on same day as preparation is completed.

-	Finish:

-	Even, smooth and of uniform colour.

-	Free from brush marks, sags, runs and other defects.

-	Cut in neatly.

M60/730	WORKSHOP COATING OF CONCEALED JOINERY SURFACES

-	General: Apply coatings to all surfaces of components.

M60/760	VARNISHING TIMBER

-	First coat:

-	Brush well in and lay off avoiding aeration.

-	Thin with white spirit.

-	Subsequent coats: Rub down lightly between coats along the grain.

M60/780	BEAD GLAZING TO COATED TIMBER

- Before glazing: Apply first two coats to rebates and beads.

M60/790	PUTTY GLAZING

-	Setting: Allow putty to set for seven days.

-	Sealing:

-	Within a further 14 days, seal with an oil based primer.

-	Fully protect putty with coating system as soon as it is sufficiently hard.

-	Extend finishing coats on to glass up to sight line.