H21	TIMBER WEATHERBOARDING

To be read with Preliminaries/ General conditions.

H21/115	VERTICAL TIMBER WEATHERBOARDING, EXTERNAL AND INTERNAL (AREA G14) INCLUDING SOFFITS AT ENTRANCE

- Substrate: breathable sheathing board as clause K11/436.

- Support system: pre-treated timber battens and counterbattens, all site-cut ends to be liberally brushed with additional preservative.

-	Counterbattens:

-	Sizes: 25 x 100 mm. Counterbattens to have chamfered top & bottom edges.

-	Centres: max. 400 mm

-		Fixing: D head annular ringed shank stainless steel nails @ max. 400 mm cc.

-	Battens:

- Sizes: 25 x 50 mm. Battens to have chamfered top & bottom ends.

-	Centres: max. 400 mm

-	Fixing: D head annular ring shanked stainless steel nails @ max. 400 mm cc.

-	Boarding:

-	Quality of timber (exposed surfaces): To BS 1186-3, Section 4, Class: 1

-	Species: Imported Douglas Fir excluding sapwood

-	Profile: Rebated & chamfered boards with 45° chamfer.

-	Finished face dimension (overall width): 119 mm

-	Finished thickness: 19 mm

-	Moisture content at time of fixing: 13 – 19%

-	Method of fixing to each support: Boards to be fixed heart out. Boards to be overlapped min. 15 mm. Boards to be fixed with 2 mm gap above each board. Boards to be fixed with 2 no. min. 38 mm long D head annular ringed shank austenitic stainless steel nails per board width. Nails to be fixed min. 15mm from ends of board. Nails to avoid penetrating tongue of boards below. Nails to be driven marginally below surface.

-	Other requirements: Black insect mesh to be fixed at all open joints. Refer to drawings for details at window openings.

H21/135	TIMBER BATTENS/ COUNTERBATTENS

-	Quality of timber: Regularized softwood free from decay, insect attack (except ambrosia beetle damage) and with no knots wider than half the section width.

-	Treatment: Preservative impregnation.

-	Standard: To NBS section Z12 and British Wood Preserving and Damp-proofing Association Commodity Specification C8.

-	Type: Tanalith E

-	Moisture content: Not exceeding 20% at time of fixing.

H21/141	FIXING BATTENS/ COUNTERBATTENS TO FRAMING/ SHEATHING

-	Setting out: In straight, vertical lines at centres coincident with vertical framing members.

-	Batten/ Counterbatten length (minimum): 1200 mm.

-	Installation: Where sheathing is provided, fix through sheathing into framing. Fastener heads to finish flush with or slightly below batten face.

H21/142	FIXING BATTENS TO COUNTERBATTENS

-	Setting out: In straight, horizontal lines. Align on adjacent areas.

-	Batten/ Counterbatten length (minimum): 1200 mm.

-	Joints: Square cut, butted centrally on counterbattens and not occurring more than once in any group of four battens on any one counterbatten.

-	Installation: Fix each batten to each counterbatten. Use splay fixings at joints. Fastener heads to finish flush with or slightly below batten face.

H21/145	TREATED TIMBER

-	Surfaces exposed by minor cutting and/ or drilling: Treat with two flood coats of a solution recommended for the purpose by main treatment solution manufacturer.

H21/150	SURFACE TREATMENT

-	Finishing system: Before fixing boards, apply first coat of specified system to all surfaces. Apply liberally to end grain.

H21/160	FIXING BOARDING

-	General: Fix boards securely to give flat, true surfaces free from undulations, lipping, splits, hammer marks and protruding fasteners.

-	Movement: Allow for movement of boards and fixings to prevent cupping, springing, excessive opening of joints or other defects.

-	Heading joints: Position centrally over supports and at least two board widths apart on any one support.

-	Nail heads: Punch below surfaces that will be seen in the completed work.