M42	WOOD BLOCK/ COMPOSITION BLOCK/ MOSAIC PARQUET FLOORING

To be read with Preliminaries/ General conditions.

TYPES OF FLOORING

M42/110	NEW AREAS OF WOOD BLOCK FLOORING TO AREA G13

-	Substrate: cement/sand screed .

-	Preparation: As clause 220 .

-	Wood blocks: Free from decay, through splits and insect attack (including ambrosia beetle damage, unless permitted in the class/ grade specified).

-	Manufacturer: Contractor’s choice .

Product reference: reclaimed blocks .

-	Species: to match existing .

-	Appearance class/ Grade: to match existing .

-	Block size: to match existing .

-	Edges: to match existing .

Bottom of long edges: Chamfered/ grooved to take up surplus adhesive.

-	Finish as delivered: planed .

-	Moisture content at time of laying: 6-10% .

-	Laying:

-	Pattern: harringbone to match existing .

-	Adhesive: Lecol 5500 from Havwood Accessories .

-	Method of finishing: Sand and seal with 2 coats of varnish to match finish of existing blocks in first phase areas.

M42/110/A	EXISTING WOODBLOCK FLOORING TO AREAS G12, G13 AND G21 Sand and seal with 2 coats of varnish to match finish of existing blocks in first phase areas.

PREPARATION OF SUBSTRATES

M42/210	DRYNESS OF CONCRETE/ SCREED SUBSTRATES

-	Relative humidity above substrate when tested with a hygrometer to BS 8201, Appendix A (maximum): 75%.

-	Test points: All corners, around perimeter, and random points over area being tested.

-	Drying aids: Turned off for not less than 4 days before testing.

M42/220	CONCRETE/ SCREED SUBSTRATES

-	Finished surface: Smooth, even, and free from abrupt changes in level. Apply suitable smoothing compound, as necessary.

-	Surface regularity when checked with a 3 m straightedge with 3 mm feet at each end, placed anywhere on the surface: No gap greater than 6 mm, and straightedge not obstructed by the substrate.

-	Primer: If recommended by adhesive manufacturer, apply and allow to dry thoroughly before laying flooring.

M42/250	HACKING FOR KEY

- Specified substrates: Roughened thoroughly and evenly by pneumatic scabbling or bush hammering.

GENERAL

M42/310	ENVIRONMENTAL CONDITIONS

-	General requirements prior to starting work specified in this section: Building weathertight, wet trades completed and affected areas dried out.

-	emperature and humidity before, during and after installing strips/ boards: Maintained at levels approximating to those which will prevail after building is occupied.

M42/320	HEATING SYSTEM

-	Operating mode: Intermittent .

-	Room temperatures for which the system has been designed: 20-22 degrees C .

-	Operation up to completion: Submit proposals .

M42/350	PRODUCT SAMPLES

-	Representative samples of flooring: Submit before placing orders.

-	Type of flooring: Submit proposals .

M42/380	ACCLIMATIZATION

-	General: Before laying commences acclimatize materials by unpacking and spreading out in the spaces where they are to be laid.

-	Acclimatization period: As recommended by manufacturer, but not less than 48 hours.

LAYING/ FINISHING

M42/410	SUITABILITY OF SUBSTRATE

-	Condition prior to laying flooring: Dry and free from dust, debris, grease and other deleterious matter.

M42/450	APPEARANCE OF FINISHED FLOOR

-	General: Even distribution of colour variation and free from patchiness.

-	Flatness/ regularity when checked with a 2 m straightedge with 3 mm feet at each end, placed anywhere on the surface: Sudden irregularities not permitted. Straightedge not obstructed by flooring and no gap greater than 6 mm.

M42/510	LAYING WOOD BLOCKS

-	Setting out: Blocks laid to a symmetrical pattern. Small cut blocks kept to a minimum. Minor vertical gaps between blocks evened out.

-	Laying: Blocks fully bonded to substrate.

M42/560	ALLOWANCE FOR MOVEMENT

-	Expansion gap around perimeter of flooring: as supplier’s recommendations .

-	Gap filler: as supplier’s recommendations .

-	Spacer blocks and debris: Removed before fixing skirtings/ cover fillets.

-	Intermediate movement joints: Formed as recommended by flooring manufacturer/ supplier in agreed positions.

M42/580	SANDING AND FILLING

-	Finished surfaces: Smooth and even, free from drum marks and with a minimum of crossgrain scoring.

-	Minor cracks and gaps: Fill with a proprietary filler coloured to match flooring.

-	Dust and debris: Remove from flooring and adjacent surfaces.

M42/590	PROTECTION

-	Protective covering: hardboard with taped joints .

-	Remove at completion.