J40	FLEXIBLE SHEET TANKING/ DAMP PROOFING

To be read with Preliminaries/ General conditions.

J40/110	HARDCORE BEDS

-	Preparation: Blind with soft sand or pulverized fuel ash.

-	Thickness (minimum): 25mm .

-	Finish on completion: Smooth, consolidated bed free of sharp projections.

TYPES OF TANKING/ DAMP PROOFING

J40/120	LOOSE LAID POLYETHYLENE DAMP PROOF MEMBRANE

-	Substrate: beam & block floor

-	Membrane manufacturer: Contractor’s choice

-	Product reference: Contractor’s choice

-	Thickness/ Gauge: 2000 gauge

-	Joints: Lapped min. 150 mm.

-	Surface to be joined: Clean and dry.

- Sealing: Continuous mastic strip between overlaps; edge of top sheet sealed with jointing tape.

WORKMANSHIP

J40/310	WORKMANSHIP GENERALLY

-	Condition of substrate:

-	Clean and even textured, free from voids and sharp protrusions.

-	Moisture content: Compatible with dpm/ tanking.

-	Air and surface temperature: Do not apply sheets if below minimum recommended by membrane manufacturer.

-	Condition of membrane at completion:

-	Neat, smooth and fully supported, dressed well into abutments and around intrusions.

-	Completely impervious and continuous.

-	Undamaged. Prevent puncturing during following work.

-	Permanent overlying construction: Cover membrane as soon as possible.

J40/360	JUNCTIONS WITH PROJECTING DPCS/ CAVITY TRAYS

-	Condition of adjoining surfaces: Clean and dry.

-	Projecting dpcs/ cavity trays: Lap and fully bond/ seal with sheeting.

-	Laps (minimum): 150 mm

-	Bonding/ Sealing: Mastic tape

J40/365	JUNCTIONS WITH FLUSH DPCS/ CAVITY TRAYS

-	Preparation of adjacent dpcs/ cavity trays:

-	Expose edge where concealed.

-	Adjoining surfaces: Clean and dry.

-	Joints: Bond/ Seal sheeting to wall.

-	Dressing of sheeting beyond dpc/ cavity tray (minimum): 50 mm.

-	Bonding/ Sealing: Mastic tape

J40/370	PIPES, DUCTS, CABLES, ETC

-	Preformed collars: Recommended for the purpose by membrane manufacturer

-	Sealing: Fully bond to penetrations and sheeting.

-	Completed junctions: Impervious.