J30	LIQUID APPLIED TANKING/ DAMP PROOFING

To be read with Preliminaries/ General conditions.

TYPES OF TANKING/ DAMP PROOFING

J30/110	COLD APPLIED TANKING TO LIFT PIT

-	Substrate: Brickwork and concrete .

-	Primer: RIW Cementfill Fairing Coat and RIW Cementseal Primer .

-	Coating: RIW Cementseal .

-	Application: As manufacturer’s recommendations .

-	Reinforcement: RIW Cementjoint at all junctions of dissimilar materials .

J30/130	COLD APPLIED DAMP PROOFING TO EXISTING EXTERNAL WALL ADJACENT TO NURSERY PLAYGROUND, AND TO NEW SUB-STATION – SEE DRAWINGS

-	Substrate: Brickwork .

-	Primer: Not required.

-	Coating material.:

-	Manufacturer: RIW Ltd .

Product reference:Toughseal .

-	Application: 2 coats, coverage per coat (min) 4m2/litre .

-	Reinforcement: RIW Flexiseal in accordance with manufacturer’s recommendations

-	Blinding: not required .

EXECUTION

J30/205	SUITABILITY OF SUBSTRATE

-	Substrates generally:

-	Smooth, even textured, clean, dry and frost free.

-	Within tolerances for level and surface regularity.

-	Vertical and horizontal surfaces: Correctly prepared and free from irregularities.

-	Curing period for concrete substrates (minimum): 7 days.

-	Moisture content and stability of substrate: Must not impair integrity of finished tanking/ damp proofing.

-	Preliminary work: Complete including:

-	Chases.

-	External angles.

-	Formation of upstands and kerbs.

-	Movement joints.

-	Penetrations/ Outlets.

J30/210	COATING APPLICATION

-	Protection: Make good to surfaces to be coated

-	Adjacent surfaces exposed to view in finished work: Protect.

-	Coatings:

-	Uniform, continuous coverage. Do not allow to pool in hollows.

-	Firmly adhered to substrate and free from imperfections.

-	Prevent damage to finished coatings.

-	Penetrations: Impervious.

-	Final covering: Apply as soon as possible after coating has hardened.

J30/260	JUNCTIONS WITH DPCS

-	DPCs: Clean, all edges fully exposed.

-	Application: Fully coat dpc and overlap adjacent surfaces by (minimum) 75mm .

J30/270	BLINDING

-	Coatings: Blind whilst still tacky .

-	Surplus material: Remove when coatings are completely dry.

COMPLETION

J30/310	INSPECTION

-	Interim and final inspections: Submit reports.

J30/330	PROTECTION OF COATINGS

-	Coated surface: Clean and free from contaminants.

-	Board manufacturer: RIW .

-	Product reference: Protection board .

J30/340	BACKFILLING

-	Timing: Carry out as soon as possible after tanking and protection are complete.