Z21	MORTARS

To be read with Preliminaries/ General conditions.

CEMENT GAUGED MORTARS

Z21/110	CEMENT GAUGED MORTAR MIXES

-	Specification: Proportions and additional requirements for mortar materials are specified elsewhere.

Z21/120	SAND FOR SITE MADE CEMENT GAUGED MASONRY MORTARS

-	Standard: To BS EN 13139.

-	Grading: 0/2 (FP or MP).

-	Fines content where the proportion of sand in a mortar mix is specified as a range (e.g. 1:1: 5-6):

Lower proportion of sand: Use category 3 fines.

Higher proportion of sand: Use category 2 fines.

-	Sand for facework mortar: Maintain consistent colour and texture. Obtain from one source.

Z21/131	READY-MIXED LIME/ SAND FOR CEMENT GAUGED MASONRY MORTARS

-	Standard: To BS 4721 or BS EN 998-2.

-	Lime: Non hydraulic to BS EN 459-1.

-	Type: CL 90S.

-	Pigments for coloured mortars: To BS EN 12878.

Z21/135	SITE MADE LIME/ SAND FOR CEMENT GAUGED MASONRY MORTARS

-	Permitted use: Where a special colour is not required and in lieu of factory made ready-mixed material.

-	Lime: Non hydraulic to BS EN 459-1.

-	Type: CL 90S.

-	Mixing: Thoroughly mix lime with sand, in the dry state. Add water and mix again. Allow to stand, without drying out, for at least 16 hours before using.

Z21/160	CEMENTS FOR MORTARS

-	Cement: To BS EN 197-1 and CE marked.

-	Types:	Portland cement, 		CEM I.

Portland slag cement, 		CEM II-S.

Portland fly ash cement,	 CEM II-V or W.

-	Strength class: 32.5, 42.5 or 52.5.

-	White cement: To BS EN 197-1 and CE marked.

-	Type: Portland cement, CEM I.

-	Strength class: 52.5.

-	Sulfate resisting cement: To BS 4027 and Kitemarked.

-	Strength class: 42.5.

-	Masonry cement: To BS 5224 and Kitemarked.

-	Class: MC 12.5 (with air entraining agent).

Z21/180	ADMIXTURES FOR SITE MADE CEMENT GAUGED MORTARS

-	Air entraining (plasticizing) admixtures: To BS 4887-1 and compatible with other mortar constituents.

-	Other admixtures: Submit proposals.

-	Prohibited admixtures: Calcium chloride and any admixture containing calcium chloride.

Z21/190	RETARDED READY TO USE CEMENT GAUGED MASONRY MORTARS

-	Standard: To BS 4721 or BS EN 998-2.

-	Lime for cement:lime:sand mortars: Nonhydraulic to BS EN 459-1.

-	Type: CL 90S.

-	Pigments for coloured mortars: To BS EN 12878.

-	Time and temperature limitations: Use within limits prescribed by mortar manufacturer.

-	Retempering: Restore workability with water only within prescribed time limits.

Z21/210	MAKING CEMENT GAUGED MORTARS

-	Batching: By volume. Use clean and accurate gauge boxes or buckets.

-	Mix proportions: Based on dry sand. Allow for bulking of damp sand.

-	Mixing: Mix materials thoroughly to uniform consistency, free from lumps.

-	Mortars containing air entraining admixtures: Mix mechanically. Do not overmix.

-	Working time (maximum): Two hours at normal temperatures.

-	Contamination: Prevent intermixing with other materials.

LIME/ SAND MORTARS

Z21/310	LIME/ SAND MORTAR MIXES

-	Specification: Proportions and additional requirements for mortar materials are specified elsewhere.

Z21/320	SAND FOR LIME/ SAND MASONRY MORTARS

-	Type: Sharp, well graded.

-	Quality, sampling and testing: To BS EN 13139.

-	Grading/ Source: As specified elsewhere in relevant mortar mix items.

Z21/330	READY PREPARED LIME PUTTY

-	Type: Slaked directly from CL 90 quicklime to BS EN 459-1, using an excess of water.

-	Maturation: In pits/ containers that allow excess water to drain away.

-	Density of matured lime putty: 1.3-1.4 kg/litre.

-	Maturation period before use (minimum): ______ .

Z21/345	ADMIXTURES FOR HYDRAULIC LIME/ SAND MORTARS

-	Air entraining (plasticizing) admixtures: To BS 4887-1 and compatible with other mortar constituents.

-	Prohibited admixtures: Calcium chloride and any admixture containing calcium chloride.

Z21/360	MAKING LIME/ SAND MORTARS GENERALLY

-	Batching: By volume. Use clean and accurate gauge boxes or buckets.

-	Mixing: Mix materials thoroughly to uniform consistency, free from lumps.

-	Contamination: Prevent intermixing with other materials, including cement.

Z21/370	SITE PREPARED NONHYDRAULIC LIME/ SAND MORTARS

-	Mixing: Mix materials thoroughly by compressing, beating and chopping. Do not add water.

-	Equipment: Roller pan mixer or submit proposals.

-	Maturation period before use (maximum): ______ .

Z21/390	KNOCKING UP NONHYDRAULIC LIME/ SAND MORTARS

-	Knocking up before and during use: Achieve and maintain a workable consistency by compressing, beating and chopping. Do not add water.

-	Equipment: Roller pan mixer or submit proposals.

Z21/400	MAKING HYDRAULIC LIME/ SAND MORTARS

-	Mixing hydrated hydraulic lime:sand: Follow the lime manufacturer's recommendations for each stage of the mix.

-	Water quantity: Only sufficient to produce a workable mix.

-	Working time: Within limits recommended by the hydraulic lime manufacturer.