M30	METAL LATHING/ ANCHORED MESH REINFORCEMENT FOR PLASTERED/ RENDERED COATINGS

To be read with Preliminaries/ General conditions.

TYPES OF LATH/ REINFORCEMENT

M30/110	METAL LATH ON NEW STUDWORK WALLS

-	Substrate: Timber battens and building paper.

-	Lath: Stainless steel expanded metal

-	Grade: Not applicable .

-	Finish: Stainless steel

-	Fixing: As clause 285 .

-	Additional requirements: External angle beads and stop beads .

M30/170	METAL LATH ON SOLID SUBSTRATES

-	Substrate: Existing brickwork .

-	Lath: Stainless steel expanded metal

-	Grade: Not applicable .

-	Finish: Stainless steel

-	Fixing: As clause 285 .

-	Additional requirements: External angle beads and stop beads .

PRODUCTS

M30/215	METAL LATH

-	Internal applications: Flat, corrugated and ribbed expanded lath to BS 1369-1 or BS EN 13658-1.

-	External applications: Flat, corrugated and ribbed expanded lath to BS 1369-1 or BS EN 13658-2.

-	Galvanized steel: To BS EN 10327 and BS EN 10143.

-	Stainless steel: To BS EN 10088-1 and -2, number 1.4301 (name X5CrNi18-10).

M30/235	WIRE

-	Zinc coated mild steel wire:

-	Wire ties: Soft annealed steel tying wire.

-	Wire: To BS EN 10218-2.

-	Zinc coating: To BS EN 10244-2.

-	Stainless steel wire: To BS EN 10088-3, number 1.4301 or 1.4541 (name X5CrNi18-10 or X6CrNiTi18-10).

M30/285	FIXINGS

-	Nails: 38 x 2 mm stainless steel clout nails to BS 1202-1.

-	Staples: 32 x 2 mm stainless steel.

EXECUTION

M30/395	FIXING METAL LATH

-	Expanded metal lath to metal: 1.2 mm wire ties.

-	Ribbed metal lath to metal: 1.6 mm wire ties, or doubled 1.2 mm wire ties.

-	Welded mesh and paper lath to metal: 1.2 mm wire ties.

-	Fixing to runners: 1.2 mm wire ties.

-	Wire ties: Twist ends tightly together, cut off surplus and bend ends of wire away from face of coating.

-	Fixing to timber: Select from clout nails or staples.

M30/410	FIXING EXPANDED METAL LATH

-	Requirement: Fixed securely to give a taut, firm base for plaster or render.

-	Placement:

-	Orientation: Long way of mesh at right angles to supports.

-	Strands:

Horizontal lath: Sloping in same direction.

Vertical lath: Sloping downwards away from outer face.

-	Laps:

-	Sides (minimum): 25 mm.

-	Ends (minimum): 50 mm at supports.

-	Angles and bends: Do not locate laps within 100 mm of angles or bends.

-	Fixing:

-	Generally: 100 mm centres.

-	Sides and ends at supports: 1.2 mm wire ties.

Centres (maximum): 150 mm.

M30/420	FIXING RIBBED EXPANDED METAL LATH

-	Requirement: Fixed securely to give a taut, firm base for plaster or render.

-	Placement:

-	Orientation: Ribs at right angles to supports.

-	Apexes: Bearing on supports.

-	Laps:

-	Side ribs: Lap, press well together.

-	Ends (minimum):

50 mm at supports.

100 mm between supports.

-	Angles and bends: Do not locate laps within 100 mm of angles or bends.

-	Fixing:

-	Generally: Each rib.

-	Sides: 1.2 mm wire ties at 150 mm (maximum) centres.

-	Ends at supports: 1.6 mm wire ties at each pair of ribs.

-	Ends between supports: Two rows of 1.6 mm wire ties.

Centres (maximum): 100 mm.

M30/430	FIXING PAPER-BACKED WELDED WIRE LATH AND MESH

-	Requirement: Fixed securely to give a taut, firm base for plaster or render.

-	Placement:

-	Orientation: Fix with long dimension of sheets at right angles to supports.

-	Cross joints: Staggered.

-	Sequence: Start at bottom right hand corner, working up and to the left.

-	Laps:

-	Sides and ends (minimum): One full mesh.

-	Between supports, at angles, and in line with edges of openings: Not permitted.

-	Lath fixing generally: ______ .

M30/460	FIXING METAL LATH ON SOLID SUBSTRATES

-	Requirement: Fixed securely to give a taut, firm base for plaster or render.

-	Length and frequency of fasteners: Increase as necessary in weak areas.

-	Lath fixing generally: as manufacturer’s recommendations .