J21	MASTIC ASPHALT ROOFING/ INSULATION/ FINISHES

To be read with Preliminaries/ General conditions.

PERMANITE SPECIFICATION FOR WORKS TO MAIN ROOF AS IDENTIFIED ON DRAWINGS

Laycock Primary School, Islington, London, N1 1SW Project Reference: GJ/13090

All Communications Relating To This Specification Must Include the Project Reference

# ROOF SURVEY REPORT

| Project: | Laycock Primary School, Islington, London, N1 1SW |
| --- | --- |

| Building Use | Education |  | Roof Location | Main Flat Roofs |  |
| --- | --- | --- | --- | --- | --- |
| Roof Area (m²) | 180m² |  | Roof Access | Normal |  |
| Core Sample |  |  |  |  |  |

| - Existing System |  |
| --- | --- |
| Ceiling Type | Unknown |
| Void Depth | N/A mm |
| Void Insulation - Type and Thickness | None |
| Structural Deck - Type and Thickness | Concrete and Screed mm |
| Vapour Control | None |
| Insulation - Type and Thickness | None above roof deck level |
| Waterproofing | Mastic asphalt |
| Surface Finish | Self finished |
| Drainage - Type | Hopper head outlets |
| Perimeter Details | Upstands |
| Rooflights - Type | None |
| Service Units - Type | Various units |
| Pipe Penetrations | Service pipes |

Observations and Comments

A core sample was taken and it revealed that the existing asphalt roof has been overlaid with asphalt. The substrate was concrete with a sand/cement laid to falls.

We have allowed for 50mm insulation as it would not be feasible for 100mm insulation to be used as there would be the need for too many alterations to be made to allow the use of 100mm insulations. This goes in line with the Building Regulations part L – 2006 as highlighted below.

### Building Regulations Part L – 2006

### Refurbishment of Existing Buildings (Reference; L2B – Section 3 Paragraphs 87 – 90)

### Building Regulations Part L – 2006 requires a calculated “Target carbon dioxide Emission Rate” (TER) approach to be adopted for the refurbishment of existing buildings.  This includes all refurbishment works to the thermal element of the building (e.g. roofs and walls). It includes all re-roofing (strip and relay, patch repairs and overlay work), comprising an area in excess of 25% of the total roof area.

The regulations state that when refurbishing more than 25% of any thermal element, then reasonable provision must be made to upgrade the thermal performance, complying with a U value of 0.25W/m²K for a flat roof element. Unless such an upgrade is not technically or functionally, feasible or would not achieve a simple pay back of 15 years or less, under these circumstances, the element should be upgraded to the best standard that is technically and functionally feasible.

It is recommended that guidance be sought from the appropriate Building Control Office.

I have divided the specification into two areas low level roofs and the higher middle section between the low level roofs.

###### MATERIAL INFORMATION

## PERMAPHALT

Permaphalt is a polymer modified mastic asphalt roofing consisting of polymer modified bitumen and graded limestone aggregates. Permaphalt is covered by BBA Certificate No 89/2299. LPCB Approval 666a/01. Nominal Block Weight: 20kg.

Permaphalt Fire Performance Testing

Permaphalt systems have been tested by the Warrington Fire Research Centre and achieve the highest levels of fire performance in UK BS 476 Part 3 fire tests. Permaphalt systems also have Loss Prevention Board Certification approval.

BS 476 : Part 3 2004 – FAA

NB. For full approval data and Loss Prevention Board Certification listing see the Red Book Live at http://www.brecertification.co.uk/searchredbooklive.jsp

## PERMANITE SHEATHING FELT

Permanite Sheathing felt is a separating membrane for use beneath mastic asphalt roofing, consisting of jute fibre impregnated with bitumen. Maximum Roll Weight:  17kg Roll size: 20m²

ENERTHERM

Enertherm is a high performance CFC free rigid polyisocyanurate foam insulant surfaced on both sides with glass reinforced perforated facings. Board size 1200mm x 600mm (Nominal foam density: 30kg/m3, thermal conductivity: 0.27W/mk).

### ELASTOPROOF HIGH BOND PRIMER

Elastoproof High Bond Primer is a brush applied modified rubber latex emulsion priming solution for the preparation of concrete, brickwork, GRP and metal surfaces to receive the direct application of mastic asphalt waterproofing.

Coverage:		4-6 m²/litre

Container sizes:              5 litre/25 litre

### RUBERFOIL SBS VAPOUR BARRIER

Ruberfoil SBS vapour barrier is a bituminous membrane reinforced with Hessian and with aluminium foil core coated with SBS modified bitumen.  It is sand finished on both surfaces.  Roll weight: 33kg.  Roll size: 20m x 970mm (19.4m² Per Roll)

### SOLAFLECT

Solaflect is a solar reflective coating based on a synthetic resin solution with industrial ethanol which is pigmented with titanium dioxide and a lamina pigment. It is applied directly to mastic asphalt roofing for protection against infrared and ultra violet radiation.

Coverage:      6m²/kg/coat

Container sizes:  5kg/25kg

GOLD SPECIFICATION

| Project: | Laycock Primary School, Islington, London, N1 1SW |
| --- | --- |

| Project Location: | Main Flat Roofs |
| --- | --- |
| Structural Deck: | Concrete and Screed |
| Approximate Area: | 180m² |

SPECIFICATION NOTES

Permaphalt should be installed in accordance with BS 8000: Part 4:1989, BS 8218:1998 and Permanite installation instructions.

As the works proceed, the contractor is to ensure water tightness of the roof at all times.  Proper day joints must be formed at the end of each working day to seal the edges of the new roofing and ensure no water enters the building or damages the newly installed system.  Loose covers or mopping of bitumen is not permitted.  Materials used from the day joint, which are not part of the Permanite waterproofing system must be cut away and removed prior to continuation of the works.

Adequate protection should be afforded the newly installed Permaphalt roofing against damage caused by following trades.

Insulation materials are to be stored on a clean level surface, and protected from direct sunlight and weather.  The packaging that insulation is supplied with does not constitute adequate protection for site storage.

All preliminary work including alterations to detail items must be complete and satisfactory.

Prior to works commencing, identify in conjunction with the client, redundant roof mounted equipment, cables, pipes and rooflights.  Make good any openings to provide a satisfactory surface to receive new waterproofing.

It must be ensured that any retained components of the existing structure are sound and capable of accepting the imposed loading of the new system and associated installation procedures.

Before the works proceed the roofing contractor must ensure that the surfaces to receive the waterproofing are acceptable and that the specification conforms to the requirements.

Works must comply with the requirements of the Health and Safety at Work Act and any additional requirements of the Client.  The contractor must ensure that the works are carried out in accordance with written method statement for the project and that the appropriate risk assessments have been undertaken.

Prior to commencing work, the contractor must liaise with the client or building occupier to establish whether any hazards exist (e.g. microwave transmitters) or whether any gases or noxious/flammable fumes are vented at roof level.  If a hazard exists, an agreed working pattern must be adopted in accordance with health and safety requirements.

The contractor must liaise with the client with respect to any air intake points at roof level, to minimise the risk of any fumes or smoke from the roofing works entering the building.  In the event of air intakes being present, a working pattern agreed with the client/building occupier must be agreed prior to works commencing.

The contractor is responsible for providing adequate and appropriate fire fighting equipment for the works he is carrying out on site.  Fire fighting equipment must be appropriately positioned adjacent to where works are being undertaken.  Equipment must be in good working order and inspected/approved by competent personnel in accordance with the agreed inspection schedule.

When loading materials onto the roof, the authorised contractor must comply with the requirements of the client’s representative to prevent overloading and possible disturbance to the building structure.

At the pre-tender roof inspection stage, the roofing contractor should allow for the extent, volume and degree of difficulty in stripping and carting away from site existing waterproofing /insulating materials and debris (or surface chippings and detail work items in an overlay specification).

Raise the level of all wall and/or parapet DPC/cavity trays to ensure a minimum of upstand height of 150mm above the finished roof level of the new system.  The position of DPCs and cavity trays must always be carefully considered when adding insulation.  The installation of new DPCs and cavity trays must be carried out to the manufacturer’s recommendation, in conjunction with the client’s detailed specification.

All rainwater outlets, pipe inlets and openings to the building interior should be protected during periods of the roofing works. Liaise with the building occupier to ensure essential services are not disturbed or decommissioned unnecessarily.  NB. Protection to outlets must be removed during non-operating periods.

The roofing works to be carried out may need to comply with the requirements of Building Regulations Part L (Revision April 2006).  In all circumstances, it is recommended that advice be sought from your local Building Control Office, as to the compliance requirements for this particular project.

For latest Health and Safety Data Sheets (COSHH), regarding the specified products visit www.ikogroup.co.uk and click on full literature library to download information. Alternatively, contact IKO Ltd. Head Office.

LOW LEVEL ROOF

## PREPARATION

Surfaces to receive the new waterproofing system should be clean, smooth and dry.

Remove all existing coverings to screed level, carefully examine the screed for any damage or decay and replace with suitable materials to match existing.  Include the replacement of any damaged kerbs, gutters, expansion joints, outlets etc to ensure the satisfactory installation of the new waterproofing system.  Provide and fix new upstands where existing heights are in adequate or kerbs are missing.

A P.C. allowance should be made for the replacement of defective areas of decking/upstands.

The building must remain weatherproof at all times, the contractor must only remove areas of existing waterproofing that can be made watertight in the same day, including the provision of day joints.

Carefully remove roof hatch cover and dispose (Any roof opening must be protected)

Remove existing rainwater outlets and dispose.

Raise roof hatch kerbs openings to give a minimum upstand height of 150mm, above finished roof level. Allowance to be made for the making good of interior decoration.

A minimum 25mm x 25mm chase to be cut into the brickwork or concrete upstand, at a minimum height of 150mm above the finished level of roofing. The position of a new chase must always be carefully considered to ensure the position of existing DPCs and cavity trays is not compromised. The lower edge of the chase should be removed to form a splay in order to maintain the full thickness of asphalt at this point. Remove all dust and dirt from the chase, surfaces must be clean smooth and dry, and primed with High Bond Primer.

Install 75mm x insulation thickness tanalised timber “stop” battens, mechanically fixed to the deck, to protect and contain exposed edges of insulation at rainwater outlets, gutters, aprons etc.

Supply and fit new minimum Code 5 lead chutes at drainage points, dressing to existing external hoppers. The lead should be set into a rebate to prevent thinning of the Permaphalt.  All drainage chutes to be designed and fabricated to suit individual details, with all joints being lead burned. Wire  brush, apply light brush application of High Bond Primer and allow to dry.

Prime all brick and cementitious upstands with High Bond Primer and allow to dry. Ensure that primer is continued in to chases.

#### VAPOUR CONTROL LAYER

Ruberfoil SBS reinforced vapour barrier, fully bonded to the deck, with minimum 75mm side and end laps fully sealed, in Easy Melt Bitumen.

The installation of vapour control layers should be generally in accordance with BS 8000: BS 8217: 2005. The vapour control layer should always marry up with the waterproofing system to ensure the insulation is enveloped at all times.

#### INSULATION

Lay 50mm Enertherm CFC-free polyisocyanurate insulation fully bonded to the vapour control layer in Easy Melt Bitumen.

The thickness of insulation specified has been calculated, based on information available, to achieve a thermal transmittance (U value) of   0.43 W/m²K.

Contractor to ensure that the installed vapour control layer is dry, thoroughly cleaned and free from any debris or sharp objects that will prevent the uniform installation of the insulation or damage the subsequently applied waterproofing system.

Boards should be set back from all abutments to allow for a solid Permaphalt support plug. The width of the support plug should be at least 25mm.

Insulation boards to be closely butted to prevent cold bridging and laid so as to break the joints, and covered immediately with the waterproofing system.

Insulation board materials should be stored under cover in dry conditions on a flat platform or level bearers to protect against wetting, mechanical damage and contamination.

WATERPROOFING

Lay Permaphalt nominal 20mm thick in 2 X 10mm coats on sheathing felt separating membrane loose laid with minimum 50mm side and end laps. The surface of the final coat to be rubbed with clean coarse sand mostly passing a 600 micron sieve and mostly retained on a 212 micron sieve.

##### DETAILS

Lay Permaphalt nominal 13mm thick in 2 coats on primed brick or concrete upstands not exceeding 300mm high. Form 2 coat solid Permaphalt angle fillet at base.

Lay Permaphalt nominal 20mm thick in 3 coats on EML on sheathing felt on timber battens. Form 2 coat solid Permaphalt angle fillet at base, form fair edge at top.

Dress Permaphalt into the chase provided and point with 5:1 sand/cement mortar incorporating a PVA bonding agent.

Form Permaphalt bullnose edge to primed lead chute

##### SURFACE PROTECTION

Apply 2 coats of Solaflect solar reflective paint to Permaphalt in accordance with manufacturer’s instructions.

##### ADDITIONAL WORKS

On completion of the waterproofing, the following items should be attended to:-

All outlets and drainage pipes should be checked on completion to ensure that they are free flowing.

Provide new roof hatch, to match existing.

##### GENERAL

Permaphalt should be installed in accordance with BS 8000: Part 4:1989, BS 8218:1998 and Permanite instructions.

The laying temperature of Permaphalt should not exceed 240°c

Angle fillets should be applied in 2 coats after warming and cleaning interfaces and should measure not less than 40mm across the face.

Maintain full thickness of Permaphalt around external angles.

Gas torches shall not be permitted, except for drying substrates.

Each coat of Permaphalt should be followed by the succeeding coat without undue delay, as contamination may result in inter-layer blistering.

As the works proceed, night joints should be provided to seal the edges of the new roofing and ensure no water enters the building or damages the newly installed system.

Sand rubbing should be carried out using a wooden float. Brushing the sand is not sufficient.

Surface protection should be applied as soon as practicable.

Adequate protection should be afforded the newly installed Permaphalt roofing against damage caused by following trades.

Unless specifically approved by ourselves prior to placement, Permanite Engineered Roofing Systems can not accept responsibility for the performance of the completed Permaphalt roofing, affected by any additional items placed on the roof following completion of the Permaphalt installation.

##### GUARANTEE

Permanite Engineered Roofing Systems will on satisfactory completion of the contract, issue a GOLD 20 year (one point) insurance backed guarantee.

COMPLETION

J21/940	COMPLETION

-	Roof areas: Clean.

-	Outlets: Clear.

-	Work necessary to provide a weathertight finish: Complete.

-	Storage of materials on finished surface: Not permitted.

-	Completed mastic asphalt roof coating: Do not damage. Protect from petroleum based solvents and other chemicals, traffic and adjacent or high level working.