L40	GENERAL GLAZING

To be read with Preliminaries/ General conditions.

GENERAL REQUIREMENTS

L40/150	WORKMANSHIP GENERALLY

-	Glazing generally: To BS 6262.

-	Integrity: Glazing must be wind and watertight under all conditions with full allowance made for deflections and other movements.

-	Dimensional tolerances: Panes/ sheets to be within ± 2 mm of specified dimensions.

-	Materials:

-	Compatibility: Glass/ plastics, surround materials, sealers, primers and paints/ clear finishes to be used together to be compatible. Avoid contact between glazing panes/ units and alkaline materials such as cement and lime.

-	Protection: Keep materials dry until fixed. Protect insulating glass units and plastics glazing sheets from the sun and other heat sources.

L40/152	PREPARATION

-	Surrounds, rebates, grooves and beads: Clean and prepare before installing glazing.

L40/155	GLASS GENERALLY

-	Standards: To BS 952 and relevant parts of:

-	BS EN 572 for basic soda lime silicate glass.

-	BS EN 1096 for coated glass.

-	BS EN 1748-1-1 for borosilicate glass.

-	BS EN 1748-2-1 for ceramic glass.

-	BS EN 1863 for heat strengthened soda lime silicate glass.

-	BS EN 12150 for thermally toughened soda lime silicate safety glass

-	BS EN 12337 for chemically strengthened soda lime silicate glass.

-	BS EN 13024 for thermally toughened borosilicate safety glass.

-	BS EN ISO 12543 for laminated glass and laminated safety glass.

-	Panes/ sheets: Clean and free from obvious scratches, bubbles, cracks, rippling, dimples and other defects.

-	Edges: Generally undamaged. Shells and chips not more than 2 mm deep and extending not more than 5 mm across the surface are acceptable if ground out.

L40/165	HEAT SOAKING OF THERMALLY TOUGHENED GLASS

-	Standard: BS EN 14179.

-	Holding period (minimum): as recommended by manufacturer .

-	Mean glass temperature: 290° ± 10°C.

-	Certified evidence of treatment: Submit.

-	Designated locations: As drawings .

L40/180	BEAD FIXING WITH PINS

-	Pin spacing: Regular at maximum 150 mm centres, and within 50 mm of each corner.

-	Exposed pin heads: Punched just below wood surface.

L40/181	BEAD FIXING WITH SCREWS

-	Screw spacing: Regular at maximum 225 mm centres, and within 75 mm of each corner.

TYPES OF GLAZING

L40/230	BEAD FIXED SINGLE GLAZING TO NON FIRE RESISTING DOORS AND GLAZED PANELS

-	Pane material: 6.4mm clear float laminated.

-	Surround/ bead: Flush door, hardwood splayed beads .

-	Preparation: None.

-	Bead location: Both sides of glazing.

-	Bead fixing: 19mm Stainless steel pins at 150mm centres min. .

-	Glazing compound: Acrylic silicone suitable to receive paint finish.

-	Glazing installation:

-	Glass: Located centrally in surround using setting and location blocks and distance pieces.

-	Finished thickness of back bedding after inserting glazing (minimum): 3 mm.

-	Front bedding: Applied to fill voids.

-	Beads: Bedded in glazing compound and fixed securely.

-	Visible edge of glazing compound: Finished internally and externally with a smooth chamfer.

L40/250	BEAD FIXED SINGLE OSCURED GLAZING

-	Pane material: 6.4mm Laminated obscured

-	Surround/ bead: Flush door, hardwood splayed beads .

-	Preparation: None.

-	Bead location: Both sides of glazing.

-	Bead fixing: 25mm Stainless steel pins at 150mm centres min. .

-	Glazing compound: clear silicone

-	Glazing installation:

-	Glass: Located centrally in surround using setting and location blocks and distance pieces.

-	Finished thickness of back bedding after inserting glazing (minimum): 3 mm.

-	Front bedding: Applied to fill voids.

-	Beads: Bedded in glazing compound and fixed securely.

-	Visible edge of glazing compound: Finished externally with a smooth chamfer.

L40/371	BEAD FIXED INSULATING GLASS UNITS TO ALL NEW EXTERNAL COMBINATION WINDOWS/DOORS

-	Pane material: Pilkington Insulight Phon incorporating Pilkington K Glass to achieve max 2.2 W/m2  U value to doors and max 1.8 W/m2  U value to windows thermal Insulation, Rw 38 dB Acoustic  reduction.

-	-	Inner pane: 6.8mm Pilkington Insulight Optilam Phon low E coated to cavity side .

-	Outer pane: 6.0mm clear float

-	Cavity: 16mm Argon gas filled.

-	Surround/ bead: Window manufacturers gasket system .

-	Glazing installation:

-	Insulating unit: Located centrally in surround using setting and location blocks.

-	Glazing sections/ strips/ tapes: Applied to rebate upstands and beads in positions recommended by manufacturer.

-	Beads: Installed using sufficient pressure to compress inner and outer sections/ strips/ tapes and fixed securely.

-	Drainage and ventilation holes: Unobstructed.

L40/505	PILKINGTON PYRODUR FIRE RESISTANT TAPE/ STRIP GLAZING (SEE INTERNAL DOOR SCHEDULE)

-	Fire resistance rating: 30mins

-	Pane material: 10mm Pilkington Pyrodur

-	Orientation: To manufacturers recommendations .

-	Frame/ Surround material: Flush solid cored door

-	Beads:

-	Material: Hardwood 650lg/m3 splayed

-	Location: Both Sides, one side, see details .

-	Fixing: 38mm stainless steel pins splay fixed @ 150c/c’s . see details

-	Glazing system:

-	Tape/ Strip: Mann McGowan Pyroglaze 30 Fire seals, 20x2mm see details

-	Pointing sealant: none .

-	Installation: By a firm currently registered under a UKAS certified accreditation scheme for the installation of fire resistant glazing, in accordance with glazing manufacturer's recommendations.

L40/550	GLASS MIRRORS  TO TOILETS AND SIMILAR AREAS

-	Mirror material: Float glass, silvered to give maximum reflection, free from tarnishing, discoloration, scratches and other defects visible in the designed viewing conditions.

-	Thickness: To suit mrror size .

-	Backing: Lead foil or equal .

-	Edge treatment: Polished

-	Background: Plaster on metal firrings .

-	Fixing method: Dome headed chromium plated mirror screws.

-	Installation: Fixed accurately and securely without overtightening fasteners, to provide a flat surface giving a distortion free reflection.

L40/630	MANIFESTATION TO GLAZED DOORS AND PANELS

-	Design: To be agreed but for information see details

-	Art work: To be agreed .

-	Media: Plastic type transfer.